SUPPLEMENTARY MATERIAL

TABLE S-I. Densities ((), viscosities ((), excess molar volumes (VmE) and excess viscosities ((E) for the binary blends of CH (1) with the three esters (2) at 298.15, 308.15 and 318.15 K; x1-mole fraction of CH

| x1 | ( ×10-3/kg m-3 | (/mPa s | VmE×106/ m3 mol-1 | (E/mPa s |
| --- | --- | --- | --- | --- |
| CH (1) + MA (2) |
| T = 298.15 K |
| 0 | 0.92681 | 0.3810 | 0 | 0 |
| 0.0754 | 0.90732 | 0.3938 | 0.380 | -0.012 |
| 0.1551 | 0.88781 | 0.4094 | 0.800 | -0.025 |
| 0.2393 | 0.86932 | 0.4285 | 1.160 | -0.039 |
| 0.3286 | 0.85192 | 0.4517 | 1.440 | -0.052 |
| 0.3700 | 0.84477 | 0.4641 | 1.510 | -0.058 |
| 0.5241 | 0.82097 | 0.5242 | 1.630 | -0.071 |
| 0.6314 | 0.80660 | 0.5808 | 1.600 | -0.071 |
| 0.7460 | 0.79358 | 0.6568 | 1.389 | -0.062 |
| 0.8686 | 0.78244 | 0.7579 | 0.900 | -0.040 |
| 1 | 0.77384 | 0.8927 | 0 | 0 |
| T = 308.15 K |
| 0 | 0.91524 | 0.3491 | 0 | 0 |
| 0.0754 | 0.89370 | 0.3520 | 0.601 | -0.019 |
| 0.1551 | 0.87433 | 0.3605 | 1.051 | -0.034 |
| 0.2393 | 0.85607 | 0.3714 | 1.430 | -0.051 |
| 0.3286 | 0.83895 | 0.3876 | 1.722 | -0.066 |
| 0.3700 | 0.83151 | 0.3965 | 1.841 | -0.072 |
| 0.5241 | 0.80796 | 0.4395 | 1.997 | -0.091 |
| 0.6314 | 0.79386 | 0.4817 | 1.974 | -0.096 |
| 0.7460 | 0.78118 | 0.5432 | 1.756 | -0.090 |
| 0.8686 | 0.77086 | 0.6352 | 1.182 | -0.062 |
| 1 | 0.76433 | 0.7748 | 0 | 0 |
| T = 318.15 K |
| 0 | 0.90225 | 0.3132 | 0 | 0 |
| 0.0754 | 0.87878 | 0.3057 | 0.840 | -0.026 |
| 0.1551 | 0.85971 | 0.3094 | 1.320 | -0.042 |
| 0.2393 | 0.84136 | 0.3155 | 1.771 | -0.059 |
| 0.3286 | 0.82490 | 0.3228 | 2.050 | -0.078 |
| 0.3700 | 0.81769 | 0.3297 | 2.171 | -0.083 |
| 0.5241 | 0.79500 | 0.3556 | 2.310 | -0.108 |
| 0.6314 | 0.78152 | 0.3889 | 2.260 | -0.113 |
| 0.7460 | 0.76950 | 0.4386 | 2.000 | -0.109 |
| 0.8686 | 0.75971 | 0.5201 | 1.390 | -0.080 |
| 1 | 0.75473 | 0.6620 | 0 | 0 |
| CH (1) + EA (2) |
| T = 298.15 K |
| 0 | 0.89455 | 0.4262 | 0 | 0 |
| 0.0914 | 0.88047 | 0.4475 | 0.227 | -0.008 |
| 0.1845 | 0.86626 | 0.4640 | 0.480 | -0.024 |
| 0.2795 | 0.85214 | 0.4872 | 0.737 | -0.037 |
| 0.3764 | 0.83873 | 0.5162 | 0.919 | -0.047 |
| 0.4200 | 0.83290 | 0.5284 | 0.987 | -0.053 |
| 0.5759 | 0.81413 | 0.5909 | 1.025 | -0.061 |
| 0.6787 | 0.80289 | 0.6462 | 0.941 | -0.058 |
| 0.7836 | 0.79243 | 0.7107 | 0.746 | -0.050 |
| 0.8907 | 0.78304 | 0.7925 | 0.395 | -0.031 |
| 1 | 0.77384 | 0.8927 | 0 | 0 |
| T = 308.15 K |
| 0 | 0.88267 | 0.3874 | 0 | 0 |
| 0.0914 | 0.86805 | 0.3981 | 0.325 | -0.015 |
| 0.1845 | 0.85376 | 0.4108 | 0.627 | -0.029 |
| 0.2795 | 0.83972 | 0.4277 | 0.914 | -0.042 |
| 0.3764 | 0.82515 | 0.4456 | 1.283 | -0.057 |
| 0.4200 | 0.82079 | 0.4560 | 1.182 | -0.062 |
| 0.5759 | 0.80223 | 0.5029 | 1.248 | -0.075 |
| 0.6787 | 0.79137 | 0.5436 | 1.145 | -0.076 |
| 0.7836 | 0.78153 | 0.6009 | 0.896 | -0.066 |
| 0.8907 | 0.77239 | 0.6752 | 0.534 | -0.043 |
| 1 | 0.76433 | 0.7748 | 0 | 0 |
| T = 318.15 K |
| 0 | 0.86994 | 0.3564 | 0 | 0 |
| 0.0914 | 0.85474 | 0.3592 | 0.443 | -0.018 |
| 0.1845 | 0.84042 | 0.3635 | 0.802 | -0.036 |
| 0.2795 | 0.82682 | 0.3725 | 1.086 | -0.051 |
| 0.3764 | 0.81389 | 0.3834 | 1.297 | -0.066 |
| 0.4200 | 0.80830 | 0.3882 | 1.374 | -0.074 |
| 0.5759 | 0.79017 | 0.4202 | 1.455 | -0.089 |
| 0.6787 | 0.77936 | 0.4487 | 1.389 | -0.094 |
| 0.7836 | 0.76955 | 0.4913 | 1.175 | -0.088 |
| 0.8907 | 0.76152 | 0.5586 | 0.690 | -0.060 |
| 1 | 0.75473 | 0.6620 | 0 | 0 |
| CH (1) + MS (2) |
| T = 298.15 K |
| 0 | 1.17931 | 1.5358 | 0 | 0 |
| 0.1168 | 1.13610 | 1.4367 | 0.281 | -0.005 |
| 0.2294 | 1.09741 | 1.3549 | 0.060 | -0.001 |
| 0.3379 | 1.06052 | 1.2856 | -0.370 | 0.007 |
| 0.4425 | 1.02285 | 1.2236 | -0.719 | 0.016 |
| 0.4878 | 1.00603 | 1.1969 | -0.873 | 0.018 |
| 0.6411 | 0.94605 | 1.1096 | -1.281 | 0.025 |
| 0.7353 | 0.90552 | 1.0554 | -1.309 | 0.025 |
| 0.8265 | 0.86273 | 1.0015 | -1.052 | 0.021 |
| 0.9146 | 0.81950 | 0.9473 | -0.707 | 0.012 |
| 1 | 0.77384 | 0.8927 | 0 | 0 |
| T = 308.15 K |
| 0 | 1.16931 | 1.4024 | 0 | 0 |
| 0.1168 | 1.12552 | 1.3008 | 0.342 | -0.008 |
| 0.2294 | 1.08606 | 1.2194 | 0.200 | -0.004 |
| 0.3379 | 1.04900 | 1.1489 | -0.221 | 0.001 |
| 0.4425 | 1.01121 | 1.0892 | -0.559 | 0.011 |
| 0.4878 | 0.99471 | 1.0639 | -0.752 | 0.014 |
| 0.6411 | 0.93462 | 0.9777 | -1.141 | 0.019 |
| 0.7353 | 0.89413 | 0.9256 | -1.159 | 0.019 |
| 0.8265 | 0.85231 | 0.8744 | -1.002 | 0.016 |
| 0.9146 | 0.80851 | 0.8249 | -0.547 | 0.010 |
| 1 | 0.76433 | 0.7748 | 0 | 0 |
| T = 318.15 K |
| 0 | 1.15942 | 1.3027 | 0 | 0 |
| 0.1168 | 1.11418 | 1.1942 | 0.502 | -0.009 |
| 0.2294 | 1.07371 | 1.1084 | 0.469 | -0.007 |
| 0.3379 | 1.03673 | 1.0344 | 0.028 | -0.002 |
| 0.4425 | 0.99954 | 0.9721 | -0.388 | 0.007 |
| 0.4878 | 0.98303 | 0.9471 | -0.583 | 0.011 |
| 0.6411 | 0.92305 | 0.8612 | -0.982 | 0.017 |
| 0.7353 | 0.88228 | 0.8087 | -0.948 | 0.017 |
| 0.8265 | 0.84081 | 0.7571 | -0.812 | 0.013 |
| 0.9146 | 0.79715 | 0.7086 | -0.337 | 0.007 |
| 1 | 0.75473 | 0.6620 | 0 | 0 |

Table S-II. Free energy ((G*), enthalpy ((H*) and entropy ((S*) of activation of viscous flow for the binary blends; x1-mole fraction of CH

| x1 | (G*/kJ mol-1 | (H*/kJ mol-1 | (S*/J K-1mol-1 | R2 |
| --- | --- | --- | --- | --- |
|  | 298.15 K | 308.15 K | 318.15 K |  |  |  |
|  | CH (1) + MA (2) |
| 0 | 10.745 | 10.914 | 11.019 | 6.657 | -13.744 | 0.9928 |
| 0.0754 | 10.905 | 11.022 | 11.051 | 8.711 | -7.406 | 0.9920 |
| 0.1551 | 11.082 | 11.167 | 11.170 | 9.761 | -4.472 | 0.9944 |
| 0.2393 | 11.275 | 11.326 | 11.308 | 10.771 | -1.727 | 0.9967 |
| 0.3286 | 11.485 | 11.517 | 11.452 | 11.961 | 1.547 | 0.9947 |
| 0.3700 | 11.586 | 11.612 | 11.545 | 12.182 | 1.951 | 0.9955 |
| 0.5241 | 12.008 | 12.000 | 11.872 | 14.015 | 6.667 | 0.9942 |
| 0.6314 | 12.340 | 12.315 | 12.190 | 14.553 | 7.372 | 0.9963 |
| 0.7460 | 12.720 | 12.701 | 12.587 | 14.692 | 6.562 | 0.9968 |
| 0.8686 | 13.148 | 13.174 | 13.112 | 13.670 | 1.705 | 0.9966 |
| 1 | 13.620 | 13.746 | 13.809 | 10.793 | -9.515 | 0.9974 |
|  | CH (1) + EA (2) |
| 0 | 11.541 | 11.717 | 11.915 | 5.956 | -18.719 | 0.9990 |
| 0.0914 | 11.691 | 11.820 | 11.972 | 7.501 | -14.039 | 0.9992 |
| 0.1845 | 11.811 | 11.932 | 12.037 | 8.429 | -11.351 | 0.9997 |
| 0.2795 | 11.962 | 12.067 | 12.134 | 9.389 | -8.648 | 0.9987 |
| 0.3764 | 12.134 | 12.206 | 12.240 | 10.536 | -5.378 | 0.9990 |
| 0.4200 | 12.204 | 12.273 | 12.286 | 10.967 | -4.179 | 0.9979 |
| 0.5759 | 12.520 | 12.564 | 12.537 | 12.253 | -0.933 | 0.9973 |
| 0.6787 | 12.765 | 12.787 | 12.735 | 13.198 | 1.414 | 0.9975 |
| 0.7836 | 13.021 | 13.063 | 12.995 | 13.384 | 1.161 | 0.9947 |
| 0.8907 | 13.308 | 13.379 | 13.350 | 12.676 | -2.174 | 0.9950 |
| 1 | 13.620 | 13.746 | 13.809 | 10.793 | -9.515 | 0.9974 |
|  | CH (1) + MS (2) |
| 0 | 15.387 | 15.693 | 16.029 | 5.825 | -32.054 | 0.9977 |
| 0.1168 | 15.182 | 15.460 | 15.763 | 6.526 | -29.021 | 0.9990 |
| 0.2294 | 14.987 | 15.247 | 15.519 | 7.060 | -26.583 | 0.9997 |
| 0.3379 | 14.804 | 15.041 | 15.282 | 7.679 | -23.896 | 0.9999 |
| 0.4425 | 14.631 | 14.853 | 15.065 | 8.162 | -21.702 | 0.9999 |
| 0.4878 | 14.554 | 14.770 | 14.973 | 8.316 | -20.928 | 0.9998 |
| 0.6411 | 14.292 | 14.478 | 14.645 | 9.019 | -17.694 | 0.9996 |
| 0.7353 | 14.126 | 14.296 | 14.438 | 9.469 | -15.634 | 0.9993 |
| 0.8265 | 13.961 | 14.112 | 14.225 | 10.010 | -13.271 | 0.9988 |
| 0.9146 | 13.790 | 13.933 | 14.021 | 10.349 | -11.573 | 0.9978 |
| 1 | 13.620 | 13.746 | 13.809 | 10.793 | -9.515 | 0.9974 |

TABLE S-III. Ultrasonic speeds (u), isentropic compressibilities (κs), intermolecular free lengths (Lf), free volumes (Vf), excess isentropic compressibilities (κsE), excess intermolecular free lengths (LfE) and excess free volumes (VfE) for binary blends at 298.15 K; x1-mole fraction of CH

| x1 | u/m s-1 | κs /TPa-1 | Lf/Å | Vf×106 /m3 mol-1 | κsE /TPa-1 | LfE/Å | VfE×106 /m3 mol-1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CH (1) + MA (2) |
| 0 | 1148.5 | 8.180 | 0.5883 | 0.378 | 0 | 0 | 0 |
| 0.0754 | 1146.9 | 8.379 | 0.5954 | 0.363 | 0.189 | 0.0070 | 0.003 |
| 0.1551 | 1152.2 | 8.484 | 0.5991 | 0.351 | 0.285 | 0.0106 | 0.009 |
| 0.2393 | 1160.6 | 8.540 | 0.6011 | 0.337 | 0.332 | 0.0124 | 0.015 |
| 0.3286 | 1171.8 | 8.549 | 0.6014 | 0.321 | 0.334 | 0.0126 | 0.020 |
| 0.3700 | 1177.0 | 8.545 | 0.6012 | 0.313 | 0.327 | 0.0124 | 0.021 |
| 0.5241 | 1197.8 | 8.490 | 0.5993 | 0.276 | 0.265 | 0.0102 | 0.020 |
| 0.6314 | 1212.7 | 8.430 | 0.5972 | 0.246 | 0.202 | 0.0079 | 0.015 |
| 0.7460 | 1226.9 | 8.371 | 0.5951 | 0.213 | 0.142 | 0.0056 | 0.008 |
| 0.8686 | 1240.2 | 8.309 | 0.5929 | 0.178 | 0.080 | 0.0032 | 0.003 |
| 1 | 1253.3 | 8.227 | 0.5899 | 0.145 | 0 | 0 | 0 |
| CH (1) + EA (2) |
| 0 | 1144.3 | 8.537 | 0.6010 | 0.411 | 0 | 0 | 0 |
| 0.0914 | 1154.5 | 8.521 | 0.6004 | 0.385 | 0.013 | 0.0004 | -0.002 |
| 0.1845 | 1165.2 | 8.503 | 0.5997 | 0.367 | 0.024 | 0.0008 | 0.005 |
| 0.2795 | 1176.3 | 8.481 | 0.5990 | 0.344 | 0.032 | 0.0011 | 0.007 |
| 0.3764 | 1187.5 | 8.455 | 0.5981 | 0.318 | 0.036 | 0.0012 | 0.007 |
| 0.4200 | 1192.2 | 8.447 | 0.5978 | 0.308 | 0.042 | 0.0015 | 0.008 |
| 0.5759 | 1209.2 | 8.401 | 0.5961 | 0.263 | 0.044 | 0.0015 | 0.005 |
| 0.6787 | 1220.1 | 8.367 | 0.5949 | 0.231 | 0.041 | 0.0014 | 0.001 |
| 0.7836 | 1231.0 | 8.328 | 0.5935 | 0.202 | 0.034 | 0.0012 | -0.001 |
| 0.8907 | 1241.5 | 8.286 | 0.5920 | 0.172 | 0.025 | 0.0009 | -0.002 |
| 1 | 1253.3 | 8.227 | 0.5899 | 0.145 | 0 | 0 | 0 |
| CH (1) + MS (2) |
| 0 | 1410.9 | 4.260 | 0.4245 | 0.187 | 0 | 0 | 0 |
| 0.1168 | 1356.0 | 4.787 | 0.4500 | 0.179 | 0.056 | 0.0062 | -0.002 |
| 0.2294 | 1325.7 | 5.185 | 0.4683 | 0.174 | -0.004 | 0.0059 | -0.003 |
| 0.3379 | 1305.2 | 5.535 | 0.4839 | 0.170 | -0.098 | 0.0035 | -0.003 |
| 0.4425 | 1292.5 | 5.852 | 0.4976 | 0.165 | -0.209 | -0.0001 | -0.003 |
| 0.4878 | 1286.7 | 6.004 | 0.5040 | 0.163 | -0.243 | -0.0012 | -0.003 |
| 0.6411 | 1268.4 | 6.570 | 0.5272 | 0.156 | -0.297 | -0.0034 | -0.004 |
| 0.7353 | 1258.7 | 6.970 | 0.5430 | 0.152 | -0.271 | -0.0031 | -0.004 |
| 0.8265 | 1252.8 | 7.385 | 0.5590 | 0.149 | -0.209 | -0.0023 | -0.004 |
| 0.9146 | 1249.3 | 7.818 | 0.5751 | 0.146 | -0.105 | -0.0007 | -0.003 |
| 1 | 1253.3 | 8.227 | 0.5899 | 0.145 | 0 | 0 | 0 |

TABLE S-IV. Refractive indices (nD), molar refractions (Rm) and excess molar refractions (RmE) for the binary blends at 298.15 K; x1-mole fraction of CH

| x1 | nD | Rm×106 /m3 mol-1 | RmE×106 /m3 mol-1 |
| --- | --- | --- | --- |
| CH (1) + MA (2) |
| 0 | 1.3604 | 17.658 | 0 |
| 0.0754 | 1.3659 | 18.472 | 0.055 |
| 0.1551 | 1.3717 | 19.352 | 0.132 |
| 0.2393 | 1.3776 | 20.270 | 0.201 |
| 0.3286 | 1.3836 | 21.224 | 0.256 |
| 0.3700 | 1.3862 | 21.649 | 0.264 |
| 0.5241 | 1.3958 | 23.223 | 0.286 |
| 0.6314 | 1.4022 | 24.303 | 0.285 |
| 0.7460 | 1.4089 | 25.425 | 0.253 |
| 0.8686 | 1.4158 | 26.567 | 0.160 |
| 1 | 1.4234 | 27.730 | 0 |
| CH (1) + EA (2) |
| 0 | 1.3712 | 22.343 | 0 |
| 0.0914 | 1.3753 | 22.831 | -0.004 |
| 0.1845 | 1.3799 | 23.362 | 0.025 |
| 0.2795 | 1.3849 | 23.925 | 0.076 |
| 0.3764 | 1.3898 | 24.475 | 0.104 |
| 0.4200 | 1.3920 | 24.721 | 0.115 |
| 0.5759 | 1.4000 | 25.566 | 0.120 |
| 0.6787 | 1.4054 | 26.110 | 0.110 |
| 0.7836 | 1.4109 | 26.642 | 0.077 |
| 0.8907 | 1.4172 | 27.190 | 0.048 |
| 1 | 1.4234 | 27.730 | 0 |
| CH (1) + MS (2) |
| 0 | 1.5352 | 40.179 | 0 |
| 0.1168 | 1.5247 | 38.882 | 0.157 |
| 0.2294 | 1.5136 | 37.439 | 0.116 |
| 0.3379 | 1.5028 | 35.999 | 0.026 |
| 0.4425 | 1.4920 | 34.627 | -0.043 |
| 0.4878 | 1.4872 | 34.032 | -0.074 |
| 0.6411 | 1.4700 | 32.024 | -0.174 |
| 0.7353 | 1.4585 | 30.820 | -0.205 |
| 0.8265 | 1.4470 | 29.728 | -0.162 |
| 0.9146 | 1.4354 | 28.680 | -0.113 |
| 1 | 1.4234 | 27.730 | 0 |

Fig. S-1. A comparison between the excess molar volumes (VmE) against mole fraction of CH (x1) for the binary blends of CH (1) + some esters (2) at T = 298.15 K. The graphical points represent experimental VmE values: □, MA; ○, EA; ∆, MS. Dashed lines- PR-EOS; dotted lines-PFP; short-dotted lines-Redlich-Kister polynomial.

Fig. S-2. A comparison between the viscosities (η) obtained from various models against mole fraction of CH (x1) for the binary blends of CH (1) + : A, MA (2); B, EA (2); MS (2) at T = 298.15 K. The graphical points represent experimental η values: □, MA; ○, EA; ∆, MS. Dashed lines- BF; dotted lines-PREOS.

Fig. S-3. Standard deviations for theoretical prediction of ultrasonic speeds by different empirical relations at T = 298.15 K for the binary blends studied. Models: FL, Flory theory; IMR, Ideal mixing relation; IDR, Impedance dependence relation; CFT, Collision factor theory; NOM, Nomoto’s relation; JUN, Junjie’s relation.

Fig. S-4. Standard deviations for theoretical prediction of refractive indices by various models at T = 298.15 K for the binary blends studied. Models: LL, Lorentz-Lorenz; DG, Gladstone-Dale; AB, Arago-Biot; NEW, Newton; EYK, Eykman; EJ, Eyring-John; HEL, Heller; WEI, Weiner.