Fig. S-1. Simplified geological map of the Kovin deposit with sample locations.

Table S-I. The list of studied samples

| Field | Borehole ID | Coal Seam | Sample ID | Depth interval, m | Lithotype |
| --- | --- | --- | --- | --- | --- |
| B | KB-79 | II | 2/79 | 35.35-36.00 | Matrix coal (MC) |
|  |  | II | 3/79 | 36.80-37.60 | Mixture of matrix and xylite-rich coal (MXC) |
|  |  | II | 4/79 | 38.00-38.20 | Xylite-rich coal (XC) |
|  |  | II | 5/79 | 38.50-39.00 | Mixture of matrix and xylite-rich coal (MXC) |
|  |  | II | 6/79 | 39.00-39.10 | Mixture of matrix and mineral-rich coal (MMiC) |
|  |  | II | 8/79 | 40.15-40.65 | Mixture of matrix and xylite-rich coal (MXC) |
|  |  | III | 11/79 | 67.90-69.30 | Mixture of matrix and mineral-rich coal (MMiC) |
|  |  | III | 14/79 | 114.10-114.25 | Xylite-rich coal (XC) |
|  |  | III | 16/79 | 114.75-114.85 | Xylite-rich coal (XC) |
|  |  | III | 17/79 | 115.00-115.30 | Mixture of matrix and mineral-rich coal (MMiC) |
|  |  | III | 18/79 | 115.30-115.45 | Mixture of matrix and xylite-rich coal (MXC) |
|  |  | III | 19/79 | 115.45-116.00 | Mixture of matrix and mineral-rich coal (MMiC) |
|  |  | III | 20/79 | 116.05-116.30 | Mixture of matrix and mineral-rich coal (MMiC) |
|  | KB-91 | I | 26/91 | 22.50-24.25 | Matrix coal (MC) |
|  |  | I | 27/91 | 24.60-25.00 | Xylite-rich coal (XC) |
|  |  | I | 28/91 | 25.50-25.75 | Matrix coal (MC) |
|  |  | I | 29/91 | 25.75-26.35 | Xylite-rich coal (XC) |
|  |  | I | 30/91 | 26.35-27.65 | Matrix coal (MC) |
|  |  | I | 31/91 | 27.65-28.15 | Mixture of matrix and mineral-rich coal (MMiC) |
|  |  | II | 33/91 | 45.00-45.60 | Mixture of matrix and xylite-rich coal (MXC) |
|  |  | II | 34/91 | 45.60-46.05 | Xylite-rich coal (XC) |
|  |  | II | 36/91 | 47.05-48.35 | Mixture of matrix and mineral-rich coal (MMiC) |
|  |  | II | 38/91 | 49.30-49.50 | Xylite-rich coal (XC) |
|  |  | II | 39/91 | 50.60-50.90 | Mixture of matrix and mineral-rich coal (MMiC) |
|  |  | II | 40/91 | 51.60-52.85 | Matrix coal (MC) |
| A | GD-601 | I (Ia) | 42/601 | 42.65-43.10 | Xylite-rich coal (XC) |
|  |  | I (Ia) | 43/601 | 43.10-43.50 | Matrix coal (MC) |
|  |  | I (Ib) | 45/601 | 75.50-76.00 | Mixture of matrix and xylite-rich coal (MXC) |
|  |  | I (Ib) | 46/601 | 76.00-76.40 | Matrix coal (MC) |
|  |  | II | 48/601 | 96.40-97.00 | Mixture of matrix and mineral-rich coal (MMiC) |
|  |  | II | 49/601 | 97.00-97.50 | Matrix coal (MC) |
|  | GD-603 | I (Ia) | 50/603 | 39.00-39.55 | Xylite-rich coal (XC) |
|  |  | I (Ib) | 51/603 | 65.15-65.35 | Matrix coal (MC) |
|  |  | I (Ib) | 52/603 | 65.60-65.70 | Xylite-rich coal (XC) |
|  |  | I (Ib) | 53/603 | 65.70-66.65 | Mixture of matrix and xylite-rich coal (MXC) |
|  |  | II | 54/603 | 88.00-88.12 | Xylite-rich coal (XC) |
|  |  | II | 55/603 | 88.40-88.60 | Mixture of matrix and xylite-rich coal (MXC) |
|  |  | II | 56/603 | 88.60-88.80 | Mixture of matrix and mineral-rich coal (MMiC) |

Table S-II. The maceral composition based on mineral matter-free, vol. %

| Lithotype | Sample ID | Ta | Ub | Ac | Dd | Ge | Chf | HUMg | Sph | Cui | Rj | Suk |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MC | 2/79 | 23.0 | 14.2 | 4.0 | 40.2 | 5.4 | 2.0 | 88.8 | 1.8 | 0.2 | 0.2 | 0.2 |
| MXC | 3/79 | 24.0 | 6.6 | 16.6 | 31.4 | 2.8 | 2.2 | 83.6 | 1.8 | 0.3 | 0.0 | 0.3 |
| XC | 4/79 | 52.7 | 17.2 | 4.2 | 10.2 | 3.4 | 2.3 | 90.0 | 1.5 | 0.0 | 0.2 | 0.0 |
| MXC | 5/79 | 17.4 | 12.9 | 15.8 | 33.6 | 3.2 | 5.3 | 88.2 | 2.2 | 0.4 | 0.4 | 1.0 |
| MMiC | 6/79 | 19.1 | 17.2 | 8.9 | 34.8 | 3.6 | 6.0 | 89.6 | 1.6 | 0.2 | 0.2 | 0.2 |
| MXC | 8/79 | 15.2 | 28.4 | 7.0 | 34.4 | 3.2 | 6.8 | 95.0 | 0.6 | 0.0 | 0.4 | 0.2 |
| MMiC | 11/79 | 9.5 | 9.0 | 12.5 | 53.5 | 3.3 | 2.8 | 90.6 | 0.9 | 0.0 | 0.3 | 0.0 |
| XC | 14/79 | 18.0 | 37.2 | 2.6 | 22.4 | 4.6 | 7.2 | 92.0 | 0.7 | 0.0 | 0.5 | 0.4 |
| XC | 16/79 | 12.0 | 40.9 | 0.6 | 18.0 | 7.7 | 5.0 | 84.2 | 1.1 | 0.0 | 0.2 | 1.0 |
| MMiC | 17/79 | 2.6 | 17.2 | 8.4 | 40.6 | 4.2 | 1.6 | 74.6 | 0.6 | 0.0 | 0.0 | 0.0 |
| MXC | 18/79 | 11.2 | 25.8 | 6.8 | 30.6 | 5.4 | 1.4 | 81.2 | 1.8 | 0.4 | 0.2 | 0.2 |
| MMiC | 19/79 | 5.8 | 23.8 | 4.2 | 35.0 | 8.6 | 1.6 | 79.0 | 1.2 | 0.6 | 0.6 | 0.0 |
| MMiC | 20/79 | 4.0 | 16.8 | 5.2 | 50.8 | 4.4 | 2.3 | 83.5 | 1.0 | 0.0 | 0.8 | 0.3 |
| MC | 26/91 | 16.6 | 19.8 | 3.0 | 40.0 | 6.0 | 6.9 | 92.3 | 0.7 | 0.2 | 0.4 | 0.4 |
| XC | 27/91 | 18.4 | 38.0 | 2.2 | 24.9 | 6.2 | 2.0 | 91.7 | 0.8 | 1.0 | 0.4 | 0.4 |
| MC | 28/91 | 8.8 | 25.4 | 3.6 | 41.4 | 2.4 | 2.6 | 84.2 | 1.8 | 0.4 | 1.2 | 0.0 |
| XC | 29/91 | 23.8 | 36.1 | 3.9 | 18.2 | 2.9 | 4.6 | 89.5 | 1.2 | 0.2 | 0.8 | 0.8 |
| MC | 30/91 | 4.0 | 25.1 | 2.4 | 39.8 | 7.2 | 3.1 | 81.6 | 1.1 | 0.8 | 0.2 | 0.6 |
| MMiC | 31/91 | 3.0 | 17.3 | 7.7 | 58.4 | 3.4 | 2.3 | 92.1 | 1.0 | 0.6 | 0.8 | 0.0 |
| MXC | 33/91 | 6.3 | 29.1 | 2.2 | 39.6 | 4.0 | 5.9 | 87.1 | 0.5 | 0.2 | 1.3 | 0.2 |
| XC | 34/91 | 14.6 | 47.4 | 1.6 | 23.6 | 2.2 | 4.4 | 93.8 | 0.7 | 0.2 | 0.2 | 0.4 |
| MMiC | 36/91 | 8.0 | 29.4 | 3.6 | 32.6 | 8.4 | 4.2 | 86.2 | 1.0 | 0.2 | 0.3 | 0.0 |
| XC | 38/91 | 24.2 | 47.8 | 1.7 | 14.1 | 3.0 | 2.8 | 93.6 | 0.7 | 0.2 | 1.2 | 0.5 |
| MMiC | 39/91 | 7.2 | 22.9 | 1.3 | 41.9 | 6.1 | 2.3 | 81.7 | 1.3 | 0.5 | 0.7 | 0.0 |
| MC | 40/91 | 8.2 | 28.8 | 3.0 | 46.0 | 4.6 | 3.0 | 93.6 | 0.6 | 0.4 | 0.2 | 0.4 |
| XC | 42/601 | 22.0 | 39.1 | 3.2 | 23.7 | 5.6 | 1.4 | 95.0 | 1.0 | 0.6 | 0.5 | 0.2 |
| MC | 43/601 | 8.4 | 25.1 | 2.2 | 52.1 | 4.0 | 2.6 | 94.4 | 1.6 | 0.0 | 0.2 | 0.2 |
| MXC | 45/601 | 7.9 | 27.3 | 2.2 | 47.5 | 4.6 | 2.5 | 92.0 | 0.7 | 0.2 | 0.7 | 0.2 |
| MC | 46/601 | 5.4 | 27.5 | 0.8 | 47.6 | 1.9 | 1.6 | 84.8 | 1.8 | 0.8 | 0.2 | 0.2 |
| MMiC | 48/601 | 10.4 | 26.8 | 4.7 | 42.8 | 4.9 | 3.9 | 93.5 | 0.8 | 0.2 | 1.1 | 0.2 |
| MC | 49/601 | 9.8 | 28.2 | 3.7 | 39.5 | 4.1 | 5.6 | 90.9 | 0.2 | 0.2 | 0.4 | 1.0 |
| XC | 50/603 | 13.2 | 44.7 | 0.4 | 16.8 | 7.4 | 4.3 | 86.8 | 1.2 | 0.2 | 0.4 | 0.4 |
| MC | 51/603 | 20.0 | 45.6 | 0.2 | 17.8 | 2.6 | 3.4 | 89.6 | 1.4 | 0.4 | 0.6 | 0.2 |
| XC | 52/603 | 13.0 | 47.4 | 0.2 | 22.6 | 7.5 | 1.9 | 92.6 | 1.9 | 0.2 | 0.2 | 0.2 |
| MXC | 53/603 | 5.3 | 37.2 | 2.1 | 34.5 | 3.8 | 3.5 | 86.4 | 1.7 | 0.2 | 0.2 | 0.7 |
| XC | 54/603 | 22.7 | 44.3 | 0.2 | 20.2 | 1.5 | 3.0 | 91.9 | 1.2 | 0.2 | 2.0 | 0.2 |
| MXC | 55/603 | 15.8 | 32.0 | 1.3 | 37.6 | 1.3 | 1.4 | 89.4 | 1.7 | 0.2 | 1.6 | 0.2 |
| MMiC | 56/603 | 5.8 | 32.2 | 3.3 | 36.1 | 3.8 | 4.2 | 85.4 | 1.7 | 1.0 | 1.0 | 0.7 |
| Lithotype | Sample ID | All | Ldm | LIPn | Fo | Sfp | Maq | Fgr | Ids | INt | MMu |  |
| MC | 2/79 | 0.7 | 2.7 | 5.8 | 2.0 | 0.4 | 0.0 | 1.6 | 1.4 | 5.4 | 8.0 |  |
| MXC | 3/79 | 0.7 | 3.9 | 7.0 | 2.8 | 1.2 | 0.3 | 0.4 | 4.7 | 9.4 | 23.9 |  |
| XC | 4/79 | 0.0 | 1.9 | 3.6 | 3.0 | 0.4 | 0.2 | 0.2 | 2.6 | 6.4 | 9.9 |  |
| MXC | 5/79 | 0.0 | 3.4 | 7.4 | 0.5 | 0.4 | 0.0 | 1.8 | 1.7 | 4.4 | 8.6 |  |
| MMiC | 6/79 | 0.2 | 2.4 | 4.8 | 0.6 | 0.3 | 0.2 | 1.0 | 3.5 | 5.6 | 13.0 |  |
| MXC | 8/79 | 0.0 | 1.8 | 3.0 | 0.4 | 0.0 | 0.0 | 0.8 | 0.8 | 2.0 | 9.4 |  |
| MMiC | 11/79 | 0.3 | 1.4 | 2.9 | 1.3 | 0.7 | 0.4 | 0.9 | 3.2 | 6.5 | 29.7 |  |
| XC | 14/79 | 0.0 | 1.8 | 3.4 | 1.2 | 0.4 | 0.5 | 0.8 | 1.7 | 4.6 | 8.8 |  |
| XC | 16/79 | 0.0 | 0.3 | 2.6 | 4.2 | 3.9 | 0.2 | 0.4 | 4.5 | 13.2 | 3.3 |  |
| MMiC | 17/79 | 0.0 | 0.6 | 1.2 | 9.4 | 1.2 | 0.2 | 0.2 | 13.2 | 24.2 | 11.4 |  |
| MXC | 18/79 | 0.0 | 1.6 | 4.2 | 2.8 | 0.8 | 1.6 | 0.6 | 8.8 | 14.6 | 14.4 |  |
| MMiC | 19/79 | 0.3 | 2.2 | 4.9 | 2.8 | 1.8 | 1.2 | 0.8 | 9.5 | 16.1 | 13.5 |  |

Table S-II continued

| Lithotype | Sample ID | All | Ldm | LIPn | Fo | Sfp | Maq | Fgr | Ids | INt | MMu |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MMiC | 20/79 | 0.0 | 0.7 | 2.8 | 2.0 | 3.0 | 0.4 | 0.3 | 8.0 | 13.7 | 20.4 |
| MC | 26/91 | 0.0 | 0.4 | 2.1 | 1.0 | 0.4 | 0.4 | 1.2 | 2.6 | 5.6 | 16.8 |
| XC | 27/91 | 0.0 | 1.4 | 4.0 | 0.8 | 0.2 | 0.2 | 0.2 | 2.9 | 4.3 | 4.2 |
| MC | 28/91 | 0.2 | 3.2 | 6.8 | 2.2 | 0.2 | 0.2 | 1.0 | 5.4 | 9.0 | 5.5 |
| XC | 29/91 | 0.0 | 2.0 | 5.0 | 1.0 | 0.4 | 0.4 | 0.5 | 3.2 | 5.5 | 8.8 |
| MC | 30/91 | 0.0 | 1.0 | 3.7 | 2.4 | 0.5 | 1.2 | 0.2 | 10.4 | 14.7 | 15.0 |
| MMiC | 31/91 | 0.0 | 1.6 | 4.0 | 1.4 | 0.0 | 0.3 | 0.6 | 1.6 | 3.9 | 22.9 |
| MXC | 33/91 | 0.2 | 2.5 | 4.9 | 1.8 | 0.2 | 0.2 | 0.8 | 5.0 | 8.0 | 14.8 |
| XC | 34/91 | 0.0 | 1.7 | 3.2 | 0.2 | 0.4 | 0.0 | 1.7 | 0.7 | 3.0 | 8.1 |
| MMiC | 36/91 | 0.0 | 1.7 | 3.2 | 2.6 | 0.8 | 0.2 | 0.6 | 6.4 | 10.6 | 13.9 |
| XC | 38/91 | 0.0 | 1.4 | 4.0 | 0.7 | 0.3 | 0.0 | 0.7 | 0.7 | 2.4 | 11.4 |
| MMiC | 39/91 | 0.0 | 1.8 | 4.3 | 1.0 | 1.5 | 0.0 | 1.4 | 10.1 | 14.0 | 15.9 |
| MC | 40/91 | 0.0 | 2.4 | 4.0 | 0.2 | 0.2 | 0.2 | 1.2 | 0.6 | 2.4 | 9.3 |
| XC | 42/601 | 0.0 | 0.7 | 3.0 | 0.5 | 0.2 | 0.0 | 0.2 | 1.1 | 2.0 | 11.2 |
| MC | 43/601 | 0.0 | 1.5 | 3.5 | 0.2 | 0.4 | 0.0 | 0.2 | 1.3 | 2.1 | 7.4 |
| MXC | 45/601 | 0.5 | 1.7 | 4.0 | 0.2 | 0.7 | 0.2 | 0.9 | 2.0 | 4.0 | 12.4 |
| MC | 46/601 | 0.6 | 1.0 | 4.6 | 2.7 | 2.5 | 0.6 | 0.6 | 4.2 | 10.6 | 11.5 |
| MMiC | 48/601 | 0.2 | 1.4 | 3.9 | 0.2 | 0.5 | 0.2 | 0.2 | 1.5 | 2.6 | 15.0 |
| MC | 49/601 | 0.4 | 2.1 | 4.3 | 1.0 | 0.4 | 0.4 | 0.8 | 2.2 | 4.8 | 9.9 |
| XC | 50/603 | 0.0 | 1.4 | 3.6 | 3.2 | 1.0 | 0.4 | 0.6 | 4.4 | 9.6 | 4.6 |
| MC | 51/603 | 0.0 | 2.2 | 4.8 | 2.0 | 0.4 | 0.2 | 0.4 | 2.6 | 5.6 | 4.3 |
| XC | 52/603 | 0.0 | 0.9 | 3.4 | 0.2 | 0.8 | 0.4 | 0.8 | 1.8 | 4.0 | 5.5 |
| MXC | 53/603 | 0.2 | 3.9 | 6.9 | 0.9 | 0.2 | 0.9 | 1.2 | 3.5 | 6.7 | 19.3 |
| XC | 54/603 | 0.0 | 2.2 | 5.8 | 0.2 | 0.2 | 0.0 | 0.9 | 1.0 | 2.3 | 7.8 |
| MXC | 55/603 | 0.0 | 2.3 | 6.0 | 0.5 | 1.1 | 0.5 | 0.2 | 2.3 | 4.6 | 17.8 |
| MMiC | 56/603 | 0.0 | 2.9 | 7.3 | 1.7 | 0.7 | 0.4 | 0.4 | 4.1 | 7.3 | 19.2 |

aT – Textinite; bU – Ulminite; cA – Attrinite; dD – Densinite; eG – Gelinite; fCh – Corpohuminite; gHUM – Total huminite; hSp – Sporinite; iCu – Cutinite; jR – Resinite; kSu – Suberinite; lAl – Alginite; mLd – Liptodetrinite; nLIP – Total liptinite; oF – Fusinite; pSf – Semifusinite; qMa – Macrinite; rFg – Funginite; sId – Inertodetrinite; tIN – Total inertinite; uMM – Total mineral matter.

Table S-III. Petrographic indices and bulk organic geochemical parameters

| Lithotype | Sample ID | ΣGa /vol. % | GIb | TPIc | VId | GWIe | TOCf /% | Sg /% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MC | 2/79 | 43.85 | 1.86 | 0.93 | 0.86 | 1.35 | 56.06 | 1.88 |
| MXC | 3/79 | 30.44 | 0.84 | 0.74 | 0.65 | 1.28 | 24.23 | 1.67 |
| XC | 4/79 | 24.03 | 0.48 | 5.15 | 3.97 | 0.35 | 52.90 | 2.87 |
| MXC | 5/79 | 39.69 | 1.46 | 0.73 | 0.65 | 1.10 | 44.67 | 0.78 |
| MMiC | 6/79 | 44.43 | 1.81 | 0.98 | 0.79 | 1.27 | 20.21 | 0.51 |
| MXC | 8/79 | 52.12 | 2.97 | 1.23 | 1.03 | 1.06 | 45.79 | 3.34 |
| MMiC | 11/79 | 47.96 | 2.48 | 0.34 | 0.31 | 2.88 | 8.31 | 0.21 |
| XC | 14/79 | 51.73 | 2.86 | 2.49 | 2.05 | 0.74 | 51.64 | 1.53 |
| XC | 16/79 | 52.11 | 3.01 | 3.30 | 2.71 | 0.64 | 57.01 | 1.33 |
| MMiC | 17/79 | 44.47 | 1.77 | 0.63 | 0.49 | 2.05 | 27.16 | 0.82 |
| MXC | 18/79 | 44.58 | 2.01 | 1.06 | 0.90 | 1.18 | 43.97 | 1.45 |
| MMiC | 19/79 | 49.60 | 2.76 | 0.84 | 0.71 | 1.74 | 48.90 | 1.70 |
| MMiC | 20/79 | 51.94 | 3.66 | 0.45 | 0.43 | 3.00 | 27.52 | 2.13 |
| MC | 26/91 | 52.96 | 2.89 | 1.02 | 0.86 | 1.77 | 37.36 | 1.80 |
| XC | 27/91 | 50.31 | 2.68 | 2.17 | 1.91 | 0.64 | 50.80 | 1.98 |
| MC | 28/91 | 49.82 | 3.48 | 0.86 | 0.74 | 1.37 | 29.97 | 1.73 |
| XC | 29/91 | 43.82 | 1.86 | 2.91 | 2.36 | 0.54 | 49.29 | 1.41 |
| MC | 30/91 | 53.67 | 3.60 | 0.80 | 0.65 | 2.07 | 29.58 | 3.33 |
| MMiC | 31/91 | 56.37 | 5.72 | 0.36 | 0.35 | 3.11 | 26.10 | 4.40 |
| MXC | 33/91 | 55.86 | 4.89 | 1.03 | 0.80 | 1.71 | 39.65 | 1.46 |
| XC | 34/91 | 54.14 | 4.41 | 2.64 | 2.32 | 0.60 | 48.67 | 1.65 |
| MMiC | 36/91 | 54.10 | 3.22 | 1.21 | 0.95 | 1.44 | 26.22 | 1.35 |
| XC | 38/91 | 47.38 | 2.37 | 4.78 | 4.22 | 0.42 | 51.58 | 0.80 |
| MMiC | 39/91 | 51.74 | 3.42 | 0.77 | 0.64 | 2.11 | 39.27 | 1.00 |
| MC | 40/91 | 57.69 | 6.50 | 0.82 | 0.75 | 1.57 | 33.71 | 0.92 |
| XC | 42/601 | 49.16 | 2.40 | 2.34 | 2.23 | 0.65 | 40.44 | 2.28 |
| MC | 43/601 | 58.25 | 6.60 | 0.67 | 0.63 | 1.85 | 39.93 | 2.85 |
| MXC | 45/601 | 57.17 | 6.30 | 0.76 | 0.70 | 1.79 | 40.72 | 1.86 |
| MC | 46/601 | 53.77 | 5.90 | 0.76 | 0.76 | 1.86 | 41.38 | 1.69 |
| MMiC | 48/601 | 55.49 | 4.39 | 0.87 | 0.79 | 1.59 | 23.70 | 2.94 |
| MC | 49/601 | 55.02 | 4.41 | 1.02 | 0.86 | 1.42 | 41.01 | 0.97 |
| XC | 50/603 | 52.91 | 3.12 | 3.72 | 2.80 | 0.57 | 53.16 | 1.67 |
| MC | 51/603 | 48.49 | 2.70 | 3.90 | 3.10 | 0.43 | 57.97 | 0.82 |
| XC | 52/603 | 56.28 | 4.76 | 2.69 | 2.51 | 0.62 | 56.69 | 1.68 |
| MXC | 53/603 | 55.17 | 6.45 | 1.25 | 1.05 | 1.37 | 27.12 | 1.63 |
| XC | 54/603 | 47.72 | 2.80 | 3.44 | 3.01 | 0.48 | 56.06 | 1.67 |
| MXC | 55/603 | 49.30 | 3.59 | 1.26 | 1.22 | 1.18 | 17.14 | 1.07 |
| MMiC | 56/603 | 53.73 | 4.86 | 1.10 | 0.97 | 1.53 | 8.04 | 0.22 |
| Lithotype | Sample ID | Qgh / MJ kg-1 | Qdi / MJ kg-1 | Ash, % | Bitumen, mg (g TOC)-1 | Saturated hydrocar-bons, % | Aromatic hydrocar-bons, % | Asphaltenes+ NSOj compounds, % |
| MC | 2/79 | 25.9 | 24.8 | 19.00 | 65.99 | 1.04 | 3.39 | 95.56 |
| MXC | 3/79 | 18.9 | 17.8 | 59.84 | 87.97 | 1.94 | 2.26 | 95.81 |
| XC | 4/79 | 26.1 | 25.1 | 20.63 | 59.63 | 2.11 | 3.01 | 94.88 |
| MXC | 5/79 | 24.8 | 23.7 | 28.02 | 62.07 | 1.25 | 4.74 | 94.01 |
| MMiC | 6/79 | 17.9 | 17.0 | 63.83 | 44.25 | 0.91 | 2.13 | 96.96 |
| MXC | 8/79 | 25.1 | 23.9 | 25.70 | 36.78 | 3.21 | 2.75 | 94.04 |
| MMiC | 11/79 | 15.7 | 14.3 | 78.20 | 39.66 | 2.05 | 3.22 | 94.74 |
| XC | 14/79 | 26.3 | 25.3 | 12.62 | 52.62 | 1.08 | 2.16 | 96.76 |
| XC | 16/79 | 25.6 | 24.6 | 8.66 | 22.65 | 1.45 | 2.54 | 96.01 |
| MMiC | 17/79 | 23.5 | 22.5 | 56.29 | 39.40 | 1.75 | 0.70 | 97.54 |
| MXC | 18/79 | 24.2 | 23.3 | 27.62 | 51.75 | 1.49 | 1.19 | 97.32 |

Table S-III continued

| Lithotype | Sample ID | Qgh / MJ kg-1 | Qdi / MJ kg-1 | Ash, % | Bitumen, mg (g TOC)-1 | Saturated hydrocar-bons, % | Aromatic hydrocar-bons, % | Asphaltenes+ NSOj compounds, % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MMiC | 19/79 | 25.8 | 24.8 | 25.51 | 81.28 | 1.94 | 3.23 | 94.84 |
| MMiC | 20/79 | 21.3 | 20.3 | 58.27 | 34.78 | 2.27 | 1.70 | 96.02 |
| MC | 26/91 | 23.3 | 22.1 | 42.91 | 72.18 | 4.27 | 3.73 | 92.00 |
| XC | 27/91 | 25.1 | 24.1 | 17.90 | 48.64 | 2.50 | 2.19 | 95.31 |
| MC | 28/91 | 23.0 | 21.7 | 50.85 | 64.37 | 1.13 | 3.38 | 95.49 |
| XC | 29/91 | 25.3 | 24.2 | 20.08 | 54.20 | 0.97 | 2.27 | 96.75 |
| MC | 30/91 | 22.8 | 22.1 | 40.76 | 38.13 | 1.24 | 3.72 | 95.04 |
| MMiC | 31/91 | 21.0 | 20.1 | 52.56 | 60.52 | 1.30 | 3.26 | 95.44 |
| MXC | 33/91 | 24.3 | 23.3 | 35.95 | 75.09 | 1.28 | 1.92 | 96.81 |
| XC | 34/91 | 25.9 | 24.8 | 21.74 | 54.29 | 1.57 | 1.89 | 96.54 |
| MMiC | 36/91 | 21.2 | 19.9 | 56.11 | 131.69 | 0.60 | 1.79 | 97.62 |
| XC | 38/91 | 25.5 | 24.4 | 16.38 | 46.25 | 1.09 | 1.09 | 97.83 |
| MMiC | 39/91 | 24.4 | 23.3 | 37.05 | 73.43 | 2.10 | 3.89 | 94.01 |
| MC | 40/91 | 23.9 | 22.6 | 37.92 | 58.30 | 0.65 | 2.28 | 97.07 |
| XC | 42/601 | 24.2 | 23.2 | 31.36 | 57.62 | 10.57 | 4.38 | 85.05 |
| MC | 43/601 | 24.3 | 23.3 | 34.23 | 43.43 | 8.58 | 4.48 | 86.94 |
| MXC | 45/601 | 23.8 | 22.7 | 35.43 | 47.30 | 2.24 | 3.19 | 94.57 |
| MC | 46/601 | 23.4 | 22.5 | 24.40 | 55.28 | 1.75 | 1.75 | 96.49 |
| MMiC | 48/601 | 20.2 | 19.1 | 57.75 | 100.17 | 0.91 | 1.52 | 97.56 |
| MC | 49/601 | 24.2 | 23.1 | 34.11 | 105.33 | 2.93 | 2.05 | 95.01 |
| XC | 50/603 | 26.0 | 24.9 | 18.69 | 52.94 | 1.18 | 2.35 | 96.47 |
| MC | 51/603 | 28.3 | 27.2 | 16.86 | 36.89 | 1.24 | 2.17 | 96.59 |
| XC | 52/603 | 26.4 | 25.5 | 12.58 | 28.77 | 1.42 | 1.98 | 96.60 |
| MXC | 53/603 | 22.3 | 21.1 | 52.90 | 75.55 | 1.75 | 2.05 | 96.20 |
| XC | 54/603 | 27.8 | 26.7 | 13.85 | 64.38 | 1.42 | 2.49 | 96.09 |
| MXC | 55/603 | 21.7 | 20.9 | 54.98 | 52.94 | 2.92 | 2.50 | 94.58 |
| MMiC | 56/603 | 16.9 | 16.3 | 68.60 | 41.36 | 5.24 | 2.80 | 91.96 |

aΣG = Gelinite + Corpohuminite + 0.67 (Ulminite + Densinite), (mineral matter-free basis); bGI – Gelification Index = (Ulminite + Corpohuminite + Densinite + Macrinite)/(Textinite + Attrinite + Fusinite + Inertodetrinite); cTPI – Tissue Preservation Index = (Textinite + Ulminite + Corpohuminite + Fusinite)/(Attrinite + Densinite + Macrinite); dVI – Vegetation Index = (Telohuminite + Fusinite + Semifusinite + Cutinite + Sporinite + Suberinite + Resinite)/(Detrohuminite + Inertodetrinite + Alginite + Liptodetrinite + Other liptinites); eGWI – Groundwater Index = (Gelohuminite + Densinite + Mineral Matter)/(Telohuminite + Attrinite); fTOC – Total organic carbon content, dry basis; gS – Total sulphur content, dry basis; hQg – Gross calorific value; iQd – Net calorific value; jNSO – Polar fraction, which contains nitrogen, sulphur and oxygen compounds.

Fig. S-2. Evaluation of usefulness of investigated lithotypes in fluidized bed gasification based on petrographic composition.

For the abbreviations of parameters, see the legend of Tables I and S-II.

Fig. S-3. GI vs. TPI (a) and GWI vs. VI (b) plots.

For the abbreviations of parameters, see the legend of Tables II and S-III.

Fig. S-4. TIC (Total Ion Current) of saturated fraction typical for investigated lithotypes.

Peak assignments: n-Alkanes are labelled according to their carbon number; Pr – Pristane; Ph – Phytane; ΔPr – Pristene; D1, D2 – Isopimaradienes; D3 – Norpimarane; D4 – Beyerane; D5 – Isophyllocladene; D6 – Fichtelite; D7 – Pimarane; D8 – 16((H)-Phyllocladane; D9 – 16((H)-Kaurane; D10 – Dehydroabietane isomer; D11 – Dehydroabietane; T1 – Des-A-olean-13(18)-ene; T2 – Des-A-olean-12-ene; Std – Standard; T3 – Des-A-lupane; T4 – Des-A-urs-13(18)-ene; ββ, βα and αβ designate configurations at C-17 and C-21 in hopanes; (R) designates configuration at C-22 in hopanes.

Fig. S-5. TIC (Total Ion Current) of aromatic fraction typical for investigated lithotypes.

Peak assignments: 1 – Dihydro-ar-curcumene; 2 – Cuparene; 3 – Calamenene; 4 – Eudalene; 5 – Cadina-1(10),6,8-triene; 6 – Methyldibenzofuran; 7 – 5,6,7,8-Tetrahydrocadalene; 8 – Cadalene; 9 – Isocadalene; 10 – Phenanthrene; 11 – 19-Norabieta-8,11,13-triene; 12 – 19-Norabieta-6,8,11,13-tetraene; 13 – 16,17-Bisnordehydroabietane; 14, 15 – Hibanes; 16 – 18-Norabieta-6,8,11,13-tetraene; 17 – 18-Norabieta-8,11,13-triene; 18 – 16((H)-Phyllocladane; 19 – Fluoranthene; 20 – Dehydroabietane isomer; 21 – Dehydroabietane; 22 – Pyrene; 23 – 1,2,3,4-Tetrahydroretene; 24 – 2-Methyl, 1-(4’-methylpentyl), 6-i-propyl-naphthalene; 25 – Simonellite; 26 – Totarane; 27 – Sempervirane; 28 – Retene; 29 – 4-methyl, 4,5-Dihydropyrene; 30 – Des-A-olean-diene; Std – Standard; 31 – 2-Methylretene; 32 – 3,4,7,12a-Tetramethyl-1,2,3,4,4a,11,12,12a-octahydrochrysene; 33 – 3,3,7,12a-Tetramethyl-1,2,3,4,4a,11,12,12a-octahydrochrysene; 34 – Pentamethyldodecahydrochrysene; 35,36 – Methylchrysenes; 37 – 3,4,7-Trimethyl-1,2,3,4-tetrahydrochrysene; 38 – 3,3,7-Trimethyl-1,2,3,4-tetrahydrochrysene; 39 – Perylene; 40 – Pentanorlupa-1,3,5(10)-triene; 41 – C27Hop-17(21)-ene; 42 – D-ring monoaromatic hopane; 43 – 24,25-Dinorursa-1,3,5(10),12-tetraene; 44 – 24,25-Dinorlupa-1,3,5(10)-triene; 45 – Norlanosta(eupha)hexaene; 46 – C,D-ring diaromatic hopane; 47 – 1,2,4a,9-Tetramethyl-1,2,3,4,4a, 5,6,14b-octahydropicene; 48 – 2,2,4a,9-Tetramethyl-1,2,3,4,4a,5,6,14b-octahydropicene; 49 – 4-Methyl, 24-ethyl, 19-norcholesta-1,3,5(10)-triene; 50 – B,C,D-ring triaromatic hopane; 51 – A,B,C,D-ring tetraaromatic hopane (7-Methyl, 3’-ethyl, 1,2-cyclopentanochrysene); 52 – 1,2,9-Trimethyl-1,2,3,4-tetrahydropicene; 53 – 2,2,9-Trimethyl-1,2,3,4-tetrahydropicene; 54 – C31 Benzohopane cyclised at C-16.

Table S-IV. Contents of biomarkers, μg (g TOC)-1 and values of biomarker ratios

| Lithotype | Sample ID | Dia | Trib | n-Alkanes | Hopanoids | Steroids |
| --- | --- | --- | --- | --- | --- | --- |
| MC | 2/79 | 1139.31 | 84.63 | 590.43 | 259.21 | 25.84 |
| MXC | 3/79 | 1108.06 | 318.22 | 1483.32 | 322.86 | 13.82 |
| XC | 4/79 | 1626.55 | 131.93 | 300.02 | 499.94 | 18.87 |
| MXC | 5/79 | 2934.05 | 203.75 | 275.28 | 228.14 | 20.05 |
| MMiC | 6/79 | 613.16 | 130.70 | 373.30 | 176.00 | 33.36 |
| MXC | 8/79 | 390.34 | 155.99 | 598.21 | 312.20 | 35.09 |
| MMiC | 11/79 | 741.27 | 118.40 | 578.86 | 128.63 | 17.27 |
| XC | 14/79 | 981.63 | 55.91 | 111.70 | 243.18 | 54.84 |
| XC | 16/79 | 321.58 | 49.55 | 178.48 | 111.41 | 10.54 |
| MMiC | 17/79 | 235.91 | 40.32 | 195.62 | 53.71 | 3.45 |
| MXC | 18/79 | 667.59 | 30.43 | 296.06 | 162.14 | 20.43 |
| MMiC | 19/79 | 1030.30 | 15.60 | 507.78 | 263.41 | 15.13 |
| MMiC | 20/79 | 691.39 | 111.94 | 292.94 | 220.98 | 27.81 |
| MC | 26/91 | 3463.61 | 84.66 | 567.22 | 417.51 | 45.51 |
| XC | 27/91 | 1544.68 | 77.73 | 179.78 | 135.10 | 23.63 |
| MC | 30/91 | 1152.86 | 206.61 | 149.17 | 213.27 | 25.20 |
| MMiC | 36/91 | 1973.07 | 187.79 | 255.32 | 143.52 | 15.22 |
| XC | 38/91 | 361.40 | 92.68 | 251.35 | 93.81 | 14.46 |
| MMiC | 39/91 | 1228.42 | 277.47 | 493.94 | 355.86 | 28.80 |
| MC | 40/91 | 439.23 | 196.65 | 529.10 | 152.65 | 27.95 |
| MXC | 45/601 | 1297.23 | 63.75 | 248.43 | 148.95 | 25.00 |
| MC | 46/601 | 401.86 | 90.64 | 639.55 | 187.27 | 9.21 |
| MMiC | 48/601 | 1154.87 | 133.22 | 104.93 | 59.10 | 17.27 |
| MC | 49/601 | 2603.85 | 59.40 | 708.22 | 239.95 | 22.39 |
| MC | 51/603 | 343.12 | 64.56 | 239.35 | 139.64 | 10.04 |
| XC | 52/603 | 286.72 | 65.96 | 263.16 | 156.83 | 33.57 |
| MXC | 53/603 | 1176.59 | 149.07 | 458.98 | 288.81 | 21.11 |
| XC | 54/603 | 1986.93 | 52.67 | 62.40 | 93.62 | 12.36 |
| MXC | 55/603 | 1842.38 | 124.73 | 388.71 | 117.31 | 8.78 |
| MMiC | 56/603 | 1278.70 | 130.57 | 1076.70 | 301.19 | 8.56 |
| Lithotype | Sample ID | Proportion of Di | Diterpenoids/ n-Alkanes | Di/(Di+Tri) | Aromatic Di | Perylene |
| MC | 2/79 | 0.54 | 1.93 | 0.931 | 215.68 | 7.36 |
| MXC | 3/79 | 0.34 | 0.75 | 0.777 | 182.78 | 23.16 |
| XC | 4/79 | 0.63 | 5.42 | 0.925 | 481.57 | 18.16 |
| MXC | 5/79 | 0.80 | 10.66 | 0.935 | 408.89 | 21.42 |
| MMiC | 6/79 | 0.46 | 1.64 | 0.824 | 192.67 | 14.50 |
| MXC | 8/79 | 0.26 | 0.65 | 0.714 | 157.46 | 3.60 |
| MMiC | 11/79 | 0.47 | 1.28 | 0.862 | 139.40 | 9.44 |
| XC | 14/79 | 0.68 | 8.79 | 0.946 | 148.89 | 7.03 |
| XC | 16/79 | 0.48 | 1.80 | 0.866 | 43.90 | 1.94 |
| MMiC | 17/79 | 0.45 | 1.21 | 0.854 | 97.99 | 3.65 |
| MXC | 18/79 | 0.57 | 2.25 | 0.956 | 135.81 | 7.40 |
| MMiC | 19/79 | 0.56 | 2.03 | 0.985 | 117.19 | 0.57 |
| MMiC | 20/79 | 0.51 | 2.36 | 0.861 | 384.65 | 19.87 |
| MC | 26/91 | 0.76 | 6.11 | 0.976 | 213.45 | 2.36 |
| XC | 27/91 | 0.79 | 8.59 | 0.952 | 165.34 | 4.26 |
| MC | 30/91 | 0.66 | 7.73 | 0.848 | 383.88 | 15.68 |
| MMiC | 36/91 | 0.77 | 7.73 | 0.913 | 280.98 | 24.99 |
| XC | 38/91 | 0.44 | 1.44 | 0.796 | 48.69 | 4.41 |

Table S-IV continued

| Lithotype | Sample ID | Proportion of Di | Diterpenoids/ n-Alkanes | Di/(Di+Tri) | Aromatic Di | Perylene |
| --- | --- | --- | --- | --- | --- | --- |
| MMiC | 39/91 | 0.52 | 2.49 | 0.816 | 122.27 | 20.92 |
| MC | 40/91 | 0.33 | 0.83 | 0.691 | 97.65 | 16.64 |
| MXC | 45/601 | 0.73 | 5.22 | 0.953 | 173.16 | 8.19 |
| MC | 46/601 | 0.30 | 0.63 | 0.816 | 56.51 | 3.69 |
| MMiC | 48/601 | 0.79 | 11.01 | 0.897 | 366.77 | N.D.c |
| MC | 49/601 | 0.72 | 3.68 | 0.978 | 100.47 | 8.49 |
| MC | 51/603 | 0.43 | 1.43 | 0.842 | 71.38 | 5.26 |
| XC | 52/603 | 0.36 | 1.09 | 0.813 | 35.67 | 2.06 |
| MXC | 53/603 | 0.56 | 2.56 | 0.888 | 147.25 | 15.51 |
| XC | 54/603 | 0.90 | 31.84 | 0.974 | 377.30 | 7.12 |
| MXC | 55/603 | 0.74 | 4.74 | 0.937 | 139.48 | 11.63 |
| MMiC | 56/603 | 0.46 | 1.19 | 0.907 | 135.59 | 20.04 |

aDi – Diterpenoids; bTri – Non-hopanoid triterpenoids; cN.D. – Not determined.

Note: Biomarkers in the samples 28/91, 29/91, 31/91, 33/91, 34/91, 42/601, 43/601 and 50/603 have not been analysed.

Table S-V. The δ13C values of individual diterpenoids and non-hopanoid triterpenoids of selected samples

| Lithotype | Sample ID | Beyerane | Pimarane | 16α(H)-Phyllocladane | Dehydroabietane | Simonellite | Retene | 24,25-Dinorlupa-1,3,5(10)-triene | 2,2,4a,9-Tetramethyl-1,2,3,4,4a,5,6,14b-octahydropicene |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MC | 2/79 | -25.3 | -25.9 | -26.9 | -25.5 | -25.9 | -27.6 | -28.1 | N.D.a |
| MXC | 3/79 | N.D. | N.D. |  | -26.4 | -26.8 | -28.3 | -28.9 | -30.7 |
| XC | 4/79 | -25.3 | -25.9 | -26.3 | -26.4 | -26.9 | N.D. | -29.3 | N.D. |
| MXC | 5/79 | N.D. | N.D. | N.D. | -27.0 | -27.4 | N.D. | N.D. | N.D. |
| MMiC | 6/79 | N.D. | N.D. | N.D. | -26.8 | -26.7 | N.D. | N.D. | N.D. |
| MXC | 8/79 | -26.0 | -25.4 | -26.9 | N.D. | N.D. | N.D. | N.D. | N.D. |
| MMiC | 11/79 | -26.9 | -27.4 | -27.3 | -25.2 | -25.2 | N.D. | -29.3 | -30.5 |
| XC | 16/79 | -27.3 | -27.0 | -26.7 | -26.6 | -27.3 | -28.1 | -28.2 | -30.0 |
| MXC | 18/79 | N.D. | N.D. | N.D. | -27.0 | -27.5 | N.D. | N.D. | N.D. |
| XC | 27/91 | -25.8 | -26.4 | -26.4 | -27.4 | -28.2 | N.D. | -30.3 | N.D. |
| MC | 30/91 | -25.1 | -25.9 | -26.0 | -27.2 | -28.1 | -29.3 | N.D. | -30.3 |
| MXC | 33/91 | -26.0 | -26.1 | -26.1 | -25.8 | -26.2 | N.D. | -29.6 | N.D. |
| XC | 34/91 | -25.8 | -26.1 | -26.6 | -26.8 | -26.8 | -28.1 | -29.2 | -29.6 |
| XC | 38/91 | -26.3 | -27.5 | -27.8 | -26.4 | -26.6 | -29.6 | -29.0 | -30.0 |
| MC | 40/91 | -25.5 | -26.2 | -26.9 | -26.7 | -26.9 | -27.9 | -29.2 | -29.8 |
| MXC | 45/601 | -25.7 | -26.5 | -26.8 | -27.0 | -26.5 | -28.9 | -27.4 | -27.8 |
| MC | 46/601 | -26.1 | -25.7 | -26.4 | -27.1 | -27.3 | N.D. | -28.6 | -29.1 |
| MMiC | 48/601 | -25.6 | -25.6 | -27.1 | -27.2 | -28.4 | -28.5 | -27.9 | -27.9 |
| MC | 49/601 | -27.0 | -27.0 | -27.4 | -27.1 | -27.7 | N.D. | -27.6 | -28.5 |
| XC | 50/603 | -26.1 | -27.1 | -26.3 | -27.5 | -27.8 | N.D. | -28.6 | -28.7 |
| MC | 51/603 | -25.6 | -26.0 | -26.9 | -26.7 | -25.9 | -28.0 | N.D. | -28.5 |
| XC | 52/603 | N.D. | N.D. | N.D. | -27.2 | -26.7 | -30.7 | -28.6 | -29.9 |
| MXC | 53/603 | N.D. | N.D. | N.D. | -26.2 | -26.4 | N.D. | -29.7 | -29.8 |
| XC | 54/603 | -26.9 | -26.74 | -27.3 | -27.0 | -28.1 | -27.4 | -28.1 | -28.6 |
| MMiC | 56/603 | -25.8 | -26.64 | -26.7 | -25.5 | -25.8 | -28.2 | N.D. | N.D. |

aN.D. – Not determined.

Fig. S-6. Average carbon isotopic compositions of individual biomarkers for investigated lithotypes.

Beyer. – Beyerane; Pim. – Pimarane; 16((H)-Phyl. – 16((H)-Phyllocladane; Dehab. – Dehydroabietane; Simonel. – Simonellite; Dinorlupatriene – 24,25-Dinorlupa-1,3,5(10)-triene; Tetramethyloctahydropicene – 2,2,4a,9-Tetramethyl-1,2,3,4,4a,5,6,14b-octahydropicene; β designates configuration at C-17 in C27 hopane; ββ designate configurations at C-17 and C-21 in C29 hopane; D-MH – D-ring monoaromatic hopane; ABCD-TeH – A,B,C,D-ring tetraaromatic hopane.

Table S-VI. Parameters calculated from distributions and abundances of n-alkanes and sterenes, and contents of main individual hopanoids, μg (g TOC)-1

| Lithotype | Sample ID | CPIa | Proportion of C15-C20 n-alkanes | Proportion of C21-C25 n-alkanes | Proportion of C26-C35 n-alkanes | C30 Hop-17(21)-ene | C27 17((H)-Hopane |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MC | 2/79 | 5.47 | 0.08 | 0.16 | 0.76 | 87.09 | 9.95 |
| MXC | 3/79 | 4.88 | 0.04 | 0.35 | 0.62 | 102.17 | 27.56 |
| XC | 4/79 | 1.67 | 0.03 | 0.23 | 0.73 | 72.31 | 13.73 |
| MXC | 5/79 | 2.59 | 0.04 | 0.16 | 0.80 | 57.75 | 6.36 |
| MMiC | 6/79 | 2.44 | 0.10 | 0.20 | 0.70 | 68.37 | 9.81 |
| MXC | 8/79 | 4.05 | 0.07 | 0.24 | 0.69 | 112.92 | 21.39 |
| MMiC | 11/79 | 4.38 | 0.13 | 0.33 | 0.54 | 35.55 | 10.63 |
| XC | 14/79 | 3.51 | 0.12 | 0.23 | 0.65 | 66.89 | 8.43 |
| XC | 16/79 | 1.24 | 0.06 | 0.28 | 0.66 | 40.77 | 7.38 |
| MMiC | 17/79 | 2.78 | 0.20 | 0.32 | 0.47 | 9.01 | 6.39 |
| MXC | 18/79 | 2.97 | 0.11 | 0.25 | 0.64 | 48.38 | 11.50 |
| MMiC | 19/79 | 3.35 | 0.07 | 0.35 | 0.58 | 81.34 | 19.30 |
| MMiC | 20/79 | 3.25 | 0.09 | 0.32 | 0.59 | 22.68 | 7.06 |
| MC | 26/91 | N.D.e | 0.09 | 0.25 | 0.66 | 129.77 | 45.38 |
| XC | 27/91 | 5.72 | 0.12 | 0.18 | 0.70 | 21.81 | 5.00 |
| MC | 30/91 | 1.23 | 0.14 | 0.23 | 0.62 | 17.20 | 7.98 |
| MMiC | 36/91 | 2.39 | 0.13 | 0.51 | 0.36 | 29.33 | 2.36 |
| XC | 38/91 | 2.86 | 0.07 | 0.27 | 0.66 | 24.16 | 4.76 |
| MMiC | 39/91 | 6.89 | 0.19 | 0.20 | 0.61 | 78.48 | 107.53 |
| MC | 40/91 | 3.06 | 0.08 | 0.18 | 0.73 | 70.82 | 10.01 |
| MXC | 45/601 | 3.26 | 0.14 | 0.19 | 0.66 | 46.45 | 10.83 |
| MC | 46/601 | 6.95 | 0.08 | 0.26 | 0.66 | 66.28 | 25.61 |
| MMiC | 48/601 | 2.45 | 0.18 | 0.28 | 0.53 | 16.72 | 5.49 |
| MC | 49/601 | 5.73 | 0.20 | 0.22 | 0.57 | 129.99 | 19.34 |
| MC | 51/603 | 1.26 | 0.11 | 0.24 | 0.65 | 31.22 | 9.13 |
| XC | 52/603 | 3.71 | 0.07 | 0.35 | 0.58 | 33.40 | 11.80 |
| MXC | 53/603 | 3.37 | 0.11 | 0.23 | 0.66 | 82.76 | 18.60 |
| XC | 54/603 | 4.85 | 0.18 | 0.26 | 0.56 | 15.71 | 3.96 |
| MXC | 55/603 | 4.67 | 0.31 | 0.23 | 0.46 | 21.10 | 9.51 |
| MMiC | 56/603 | 2.87 | 0.20 | 0.25 | 0.54 | 0.00 | 43.84 |
| Lithotype | Sample ID | C29 17((H)21((H)-Hopane | C31 17((H)21((H) 22(R)-Hopane | C28 28.30-Bisnorneohop-13(18)-ene | C27 Sb /% | C28 Sc /% | C29 Sd /% |
| MC | 2/79 | 8.87 | 0.00 | 14.60 | 1.43 | 4.03 | 94.54 |
| MXC | 3/79 | 15.47 | 8.73 | 12.04 | 2.64 | 2.76 | 94.6 |
| XC | 4/79 | 8.25 | 172.00 | 6.15 | 5.67 | 11.20 | 83.13 |
| MXC | 5/79 | 4.52 | 10.40 | 2.84 | 2.76 | 12.50 | 84.74 |
| MMiC | 6/79 | 5.32 | 21.21 | 3.90 | 1.69 | 6.23 | 92.08 |
| MXC | 8/79 | 9.41 | 41.01 | 19.40 | 0.69 | 7.48 | 91.83 |
| MMiC | 11/79 | 8.18 | 7.33 | 11.45 | 8.24 | 11.04 | 80.73 |
| XC | 14/79 | 4.02 | 41.11 | 16.67 | 0.71 | 6.29 | 93.00 |
| XC | 16/79 | 3.02 | 2.85 | 23.08 | 0.59 | 2.08 | 97.33 |
| MMiC | 17/79 | 0.00 | 10.22 | 0.00 | 1.53 | 8.34 | 90.13 |
| MXC | 18/79 | 8.25 | 4.53 | 10.45 | 1.84 | 9.66 | 88.5 |
| MMiC | 19/79 | 10.24 | 22.54 | 15.31 | 1.00 | 7.03 | 91.98 |
| MMiC | 20/79 | 4.84 | 6.87 | 6.78 | 0.69 | 9.55 | 89.76 |
| MC | 26/91 | 27.89 | 43.79 | 30.55 | N.D. | N.D. | N.D. |
| XC | 27/91 | 3.47 | 5.31 | 7.93 | 1.33 | 7.40 | 91.26 |

Table S-VI continued

| Lithotype | Sample ID | C29 17((H)21((H)-Hopane | C31 17((H)21((H) 22(R)-Hopane | C28 28.30-Bisnorneohop-13(18)-ene | C27 Sb /% | C28 Sc /% | C29 Sd /% |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MC | 30/91 | 4.83 | 4.26 | 3.48 | 3.35 | 10.05 | 86.60 |
| MMiC | 36/91 | 6.02 | 3.88 | 12.94 | 2.56 | 8.92 | 88.52 |
| XC | 38/91 | 4.31 | 5.41 | 7.34 | 1.43 | 9.99 | 88.58 |
| MMiC | 39/91 | 16.22 | 18.66 | 16.31 | 0.58 | 4.01 | 95.41 |
| MC | 40/91 | 6.57 | 7.52 | 24.58 | 0.85 | 6.52 | 92.63 |
| MXC | 45/601 | 6.40 | 1.47 | 6.38 | 1.45 | 4.85 | 93.70 |
| MC | 46/601 | 15.85 | 2.94 | 9.69 | 0.95 | 5.65 | 93.40 |
| MMiC | 48/601 | 1.96 | 0.79 | 0.81 | 3.39 | 6.63 | 89.98 |
| MC | 49/601 | 10.32 | 5.48 | 11.28 | 1.25 | 6.50 | 92.25 |
| MC | 51/603 | 4.83 | 31.38 | 4.55 | 1.63 | 7.91 | 90.46 |
| XC | 52/603 | 7.05 | 2.46 | 27.33 | 1.72 | 2.88 | 95.40 |
| MXC | 53/603 | 11.08 | 8.88 | 13.87 | 1.84 | 7.41 | 90.76 |
| XC | 54/603 | 1.97 | 11.65 | 1.24 | 1.61 | 10.64 | 87.75 |
| MXC | 55/603 | 5.94 | 4.49 | 5.19 | 2.99 | 7.57 | 89.44 |
| MMiC | 56/603 | 24.49 | 47.94 | 38.34 | 2.68 | 5.52 | 91.80 |

aCPI – Carbon Preference Index determined for distribution of n-alkanes C23-C33, CPI = 1/2 [Σodd(n-C23 - n-C33)/Σeven(n-C22 - n-C32) + Σodd(n-C23 - n-C33)/Σeven(n-C24 - n-C34)]; bC27 S = 100xC27(Δ2 + Δ4 + Δ5)-Sterenes/Σ(C27-C29)(Δ2 + Δ4 + Δ5)-Sterenes; cC28 S = 100xC28(Δ2 + Δ4 + Δ5)-Sterenes/Σ(C27-C29)(Δ2 + Δ4 + Δ5)-Sterenes; dC29 S = 100xC29(Δ2 + Δ4 + Δ5)-Sterenes/Σ(C27-C29)(Δ2 + Δ4 + Δ5)-Sterenes; eN.D. – Not determined.

Table S-VII. The δ13C values of individual n-alkanes and hopanoids of selected samples

| Lithotype | Sample ID | n-C25 | n-C27 | n-C29 | n-C31 | n-C33 | C30 Hop-17(21)-ene |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MC | 2/79 | -30.2 | -31.5 | -31.7 | -31.8 | -30.2 | -44.9 |
| MXC | 3/79 | N.D. | N.D. | N.D. | N.D. | N.D. | N.D. |
| XC | 4/79 | -29.7 | -31.4 | -31.2 | -31.7 | -30.5 | -39.0 |
| MXC | 5/79 | N.D. | N.D. | N.D. | N.D. | N.D. | N.D. |
| MMiC | 6/79 | N.D. | N.D. | N.D. | N.D. | N.D. | N.D. |
| MXC | 8/79 | -30.2 | -30.9 | -31.1 | -31.5 | -31.3 | -41.7 |
| MMiC | 11/79 | -29.7 | -30.6 | -30.9 | -29.2 | -31.0 | -45.8 |
| XC | 16/79 | -27.2 | -29.1 | -28.9 | -29.7 | -29.0 | -39.9 |
| MXC | 18/79 | N.D. | N.D. | N.D. | N.D. | N.D. | N.D. |
| XC | 27/91 | -29.1 | -30.7 | -30.6 | -31.4 | -30.2 | -39.1 |
| MC | 30/91 | -29.7 | -30.7 | -30.0 | -30.2 | -29.4 | -41.6 |
| MXC | 33/91 | -30.5 | -31.0 | -31.7 | N.D. a | -30.7 | -46.1 |
| XC | 34/91 | -30.2 | -31.0 | -30.9 | -31.6 | -29.5 | -47.4 |
| XC | 38/91 | -28.8 | -30.1 | -30.6 | -30.8 | -30.4 | -40.3 |
| MMiC | 39/91 | N.D. | N.D. | N.D. | N.D. | N.D. | N.D. |
| MC | 40/91 | -30.2 | -31.6 | -32.0 | N.D. | -31.4 | -46.5 |
| MXC | 45/601 | -28.9 | -30.5 | -31.1 | -31.3 | -30.3 | -45.5 |
| MC | 46/601 | -28.2 | -29.4 | -29.4 | -29.5 | -30.6 | -45.5 |
| MMiC | 48/601 | -29.8 | -31.5 | -31.0 | -31.3 | -30.4 | -44.5 |
| MC | 49/601 | -29.3 | -31.5 | -31.6 | -31.7 | -30.6 | -44.7 |
| XC | 50/603 | -29.0 | -30.2 | -29.2 | -29.7 | -29.0 | -42.4 |
| MC | 51/603 | -29.7 | -30.9 | -30.8 | -31.3 | -31.5 | -44.0 |
| XC | 52/603 | N.D. | N.D. | N.D. | N.D. | N.D. | N.D. |
| MXC | 53/603 | N.D. | N.D. | N.D. | N.D. | N.D. | N.D. |
| XC | 54/603 | N.D. | -31.9 | -31.8 | -31.8 | -30.9 | -51.3 |
| MMiC | 56/603 | -28.9 | -30.8 | -30.8 | -31.3 | -31.1 | N.D. |
| Lithotype | Sample ID | C27 17((H)-Hopane | C29 17((H)21((H)- Hopane | C31 17((H)21((H) 22(R)-Hopane | C28 28,30-Bisnorneohop-13(18)-ene | D-ring monoaromatic hopane | ABCD-ring tetraaromatic hopane |
| MC | 2/79 | -41.3 | -44.3 | N.D.a | -35.0 | N.D. | -34.1 |
| MXC | 3/79 | N.D. | N.D. | N.D. | N.D. | -34.4 | N.D. |
| XC | 4/79 | -36.8 | -38.0 | -25.9 | N.D. | -32.3 | N.D. |
| MXC | 5/79 | N.D. | N.D. | N.D. | N.D. | -37.5 | N.D. |
| MMiC | 6/79 | N.D. | N.D. | N.D. | N.D. | -32.5 | N.D. |
| MXC | 8/79 | -37.0 | -38.3 | -27.5 | -34.0 | N.D. | N.D. |
| MMiC | 11/79 | -43.9 | -44.0 | N.D. | -36.1 | N.D. | -31.3 |
| XC | 16/79 | -38.4 | -39.0 | N.D. | -34.3 | -36.0 | -33.3 |
| MXC | 18/79 | N.D. | N.D. | N.D. | N.D. | -34.9 | -33.3 |
| XC | 27/91 | N.D. | N.D. | N.D. | N.D. | -33.3 | -31.3 |
| MC | 30/91 | -38.7 | -40.7 | -25.7 | -36.3 | -33.2 | N.D. |
| MXC | 33/91 | -42.0 | -45.2 | N.D. | -35.3 | -33.4 | N.D. |
| XC | 34/91 | -38.4 | -45.1 | N.D. | -34.1 | -35.0 | -31.1 |
| XC | 38/91 | -38.2 | -39.8 | -26.1 | -34.1 | -33.1 | -30.1 |
| MMiC | 39/91 | N.D. | N.D. | N.D. | N.D. | N.D. | N.D. |
| MC | 40/91 | -41.3 | -46.0 | N.D. | -36.5 | N.D. | -32.0 |
| MXC | 45/601 | -39.0 | -40.5 | N.D. | -33.8 | -32.7 | -30.3 |
| MC | 46/601 | -37.7 | -38.4 | N.D. | -33.6 | -32.9 | -30.9 |
| MMiC | 48/601 | -42.0 | -43.8 | N.D. | N.D. | N.D. | N.D. |
| MC | 49/601 | -41.7 | -42.6 | N.D. | -36.6 | -33.7 | -31.0 |
| XC | 50/603 | -39.6 | -40.4 | -25.2 | -35.8 | -32.8 | N.D. |
| MC | 51/603 | -38.9 | -40.8 | -27.3 | N.D. | -36.5 | -31.3 |

Table S-VII continued

| Lithotype | Sample ID | C27 17((H)-Hopane | C29 17((H)21((H)- Hopane | C31 17((H)21((H) 22(R)-Hopane | C28 28,30-Bisnorneohop-13(18)-ene | D-ring monoaromatic hopane | ABCD-ring tetraaromatic hopane |
| --- | --- | --- | --- | --- | --- | --- | --- |
| XC | 52/603 | N.D. | N.D. | N.D. | N.D. | -38.0 | -32.7 |
| MXC | 53/603 | N.D. | N.D. | N.D. | N.D. | -35.8 | -32.3 |
| XC | 54/603 | N.D. | N.D. | -24.2 | N.D. | -35.9 | -34.4 |
| MMiC | 56/603 | -38.4 | -41.4 | -26.1 | N.D. | N.D. | -34.5 |

aN.D. – Not determined.

Fig. S-7. Diagenetic scheme showing the formation of series of orphan aromatic hopanoids bearing an ethyl group at C-21 from the C28 28,30-bisnorneohop-13(18)-ene.

# Comments

Figure 1 is moved from the Manuscript to the Supplementary Material. Figures in the Manuscript and the Supplementary Material are renumbered accordingly.

Table I is moved from the Manuscript to the Supplementary Material. Tables in the Manuscript and the Supplemmentry Material are renumbered accordingly.

Figure 2 is moved from the Manuscript to the Supplementary Material. Figures in the Manuscript and the Supplemmentry Material are renumbered accordingly.

Figure 3 is moved from the Manuscript to the Supplementary Material. Figures in the Manuscript and the Supplemmentry Material are renumbered accordingly.

Figure 4 is moved from the Manuscript to the Supplementary Material. Figures in the Manuscript and the Supplemmentry Material are renumbered accordingly.

Figure 5 is moved from the Manuscript to the Supplementary Material. Figures in the Manuscript and the Supplemmentry Material are renumbered accordingly.

Figure 6 is moved from the Manuscript to the Supplementary Material. Figures in the Manuscript and the Supplemmentry Material are renumbered accordingly.

Appendix from the Manusript is moved to the Supplementary Material (Figure S-7).