Dear Editor,

I am submitting a research paper entitled The physico-chemical and thermodynamic properties of the choline chloride-based deep eutectic solvents written by DRAGAN Z. TROTER, ZORAN B. TODOROVIĆ, DUŠICA R. ĐOKIĆ-STOJANOVIĆ, BILJANA S. ĐORDEVIĆ, VANJA M. TODOROVIĆ, SANDRA S. KONSTANTINOVIĆ and VLADA B. VELJKOVIĆ to your esteemed Journal.

This paper has not been previously published elsewhere. It is not under consideration for publication elsewhere, its publication is approved by all authors and that, if accepted, it will not be published elsewhere in the same form, in English or in any other language.

This work has been funded by the Ministry of Education, Science and Technological Development of the Republic of Serbia (Project III 45001).

This paper reports the physical (density, dynamic viscosity, electrical conductivity and refractive index) and thermodynamic (thermal expansion coefficient, molecular volume, lattice energy and heat capacity) properties of choline chloride (ChCl):propylene glycol, ChCl:1,3-dimethylurea and ChCl:thiourea (1:2 molar ratio) at atmospheric pressure as a function of temperature over the range of 293.15-363.15 K. Their properties were also compared with those of some already characterized ChCl-based DESs (1:2 molar ratio). The functional groups of the prepared ChCl-based DESs were analyzed by the Fourier transform infrared spectroscopy. Density, viscosity and refractive index of all DESs decrease with increasing temperature while electrical conductivity increases. Viscosity and conductivity of the tested DESs were fitted by both Arrhenius and Vogel-Tamman-Fulcher equations. The molar enthalpy, entropy and Gibbs energy of activation, determined using the Eyring theory, demonstrates the interactional factor as predominant over the structural factor for all DES systems. The fractional Walden rule, used to correlate molar conductivity and viscosity, showed an excellent linear behavior. It was shown that ChCl:propylene glycol DES had properties similar to ChCl:ethylene glycol and ChCl:glycerol DESs. However, the properties of ChCl:1,3-dimethylurea and ChCl:thiourea DESs were inferior to those of the ChCl:urea DES.

Potential reviewers:

| Zorica D. Petrović | Faculty of Science, University of Kragujevac, P.O. Box 60, 34000 Kragujevac, Serbia | zorica@kg.ac.rs |
| --- | --- | --- |
| Vladimir P. Petrović | Faculty of Science, University of Kragujevac, P.O. Box 60, 34000 Kragujevac, Serbia | vladachem@kg.ac.rs |
| Ana-Maria Popescu | “Ilie Murgulescu” Institute of Physical Chemistry, Romanian Academy, Splaiul Independentei 202, 060021 Bucharest, Romania | popescuamj@yahoo.com; ampop@chimfiz.icf.ro |

We hope the paper will meet the requirements of the Journal and be accepted for publication.

With best regards,

Vlada Veljković

Corresponding author:

Vlada B. Veljković, Faculty of Technology, University of Niš, 16000 Leskovac, Bulevar oslobodjenja 124, Serbia;

E-mail: veljkovicvb@yahoo.com

Phone: +381 16 247 203

Fax: +381 16 242 859