SUPPLEMENTARY MATERIAL TO

The physico-chemical and thermodynamic properties of the choline chloride-based deep eutectic solvents

DRAGAN Z. TROTER1, ZORAN B. TODOROVIĆ1, DUŠICA R. ĐOKIĆ-STOJANOVIĆ2,

BILJANA S. ĐORDEVIĆ1, VANJA M. TODOROVIĆ3, SANDRA S. KONSTANTINOVIĆ1 and VLADA B. VELJKOVIĆ1(

1Faculty of Technology, University of Niš, Bulevar Oslobođenja 124, 16000 Leskovac, Serbia

2Zdravlje Actavis, Vlajkova 199, 16000 Leskovac, Serbia

3Faculty of Pharmacy, University of Belgrade, Vojvode Stepe 450, 11221 Belgrade, Serbia

Fig. S-I. Schematic presentation of the ChCl-based DESs preparation.

Fig. S-2. FTIR spectra of ChCl, propylene glycol, ChCl:propylene glycol DES, ethylene glycol, ChCl:ethylene glycol DES, glycerol, ChCl:glycerol DES, urea, ChCl:urea DES, 1,3-dimethylurea, ChCl:1,3-dimethylurea DES, thiourea and ChCl:thiourea DES.

(FTIR spectra discussion: The spectra of ChCl has very strong and broad band at 3406 cm-1, which belongs to ((OH) stretching vibration. The shape of band indicates the presence of hydrogen bond, probably intramolecular, since ChCl molecule possesses both hydrogen bonding donors and acceptors. Also, the weak peak at 2846 cm-1 also confirms existence of hydrogen bonds.54 The band at 3247 cm-1 belongs to ((NH3+) vibrations, typical for charged amine derivatives, while appropriate deformation vibration ((NH3+) appears at 1660 cm-1.55 The FTIR spectra of ChCl-based DESs with propylene glycol, ethylene glycol and glycerol show a strong and broad band at (3400 cm-1 which is understandable, considering the presence of hydroxyl groups in all compounds. The shape of band suggests hydrogen bonded hydroxyl functional group, which covers all bands belonging to amine vibrations form ChCl. These spectra are very difficult to discuss, considering the overlapping of amine and hydroxyl bands, but spectra of all DESs possess all bands typical for ChCl and used alcohols.

FTIR spectra of the DES of ChCl with urea shows a strong and broad band at (3400 cm-1 which, as in ChCl spectra, belongs to hydrogen bonded hydroxyl functional group. The DES of ChCl and urea possesses band of charged amine derivatives slightly moved at 3334 and 3205 cm-1, which is expected, considering its suggested structure. On the other hand, the spectrum of DES does not have a vibration at 1684 cm-1, which can be found in the spectra of urea. This position is characteristic for carbonyl ((C=O) vibration, suggesting the enol tautomeric form of urea in this DES. As reported elsewhere56 the spectra of ChCl DESs with thiourea and 1,3-dimethylurea also has a strong and broad band at (3400 cm-1 which, as in ChCl spectra, belongs to hydrogen bonded hydroxyl functional group. FTIR spectrum of 1,3-dimethylurea has a stretching vibration at 3345 cm-1, which corresponds to secondary ((NH) group. Bands at 2344 cm-1 and 1837 cm-1 come from stretching ((C=NH+) and deformation ((C=NH+) vibrations, which confirms that the 1,3-dimethylurea is in its imidic acid form ((Z)-N,N`-dimethylcarbamimidic acid). The band belonging to stretching ((OH) vibration is widely broad at 3378 cm-1 and covers all the amine vibrations’ belonging bands. ((C-O) vibration in DES is slightly moved for (( = 11 cm-1 in DES’s spectrum, mostly because of choline-1,3-dimethylurea interaction. FTIR spectrum of thiourea possess asymmetrical and symmetrical stretching vibrations νas(NH2) + νs(NH2) at 3380 and 3273 cm-1, as well as N-C=S I, N-C=S II and N-C=S III bands at 1436, 1399 and 1084 cm-1, proving that thiourea is in its thiol form (carbamimidothioic acid).57 The slightly shift of amine deformational vibrations ((( = 11 cm-1) is also explained by choline-thiourea interaction).

TABLE I. Parameters of Eq. (1) in the temperature range of 293.15-363.15 K

| DES | Density range / kgm-3 | a / kgm-3 | b / kgm-3K-1 | MRPD / % | R2 |
| --- | --- | --- | --- | --- | --- |
| ChCl:propylene glycol | 1156.0-1191.0 | 1331.3 | - 0.482 | ±0.05 | 0.993 |
| ChCl:ethylene glycol | 1064.0-1109.0 | 1293.3 | - 0.629 | ±0.05 | 0.997 |
| ChCl:glycerol | 1147.4-1195.1 | 1402.2 | - 0.707 | ±0.13 | 0.989 |
| ChCl:urea | 1161.1-1182.9 | 1269.0 | - 0.298 | ±0.07 | 0.985 |
| ChCl:1,3-dimethylureaa | 1061.2-1362.6 | 3168.0 | - 5.7929 | ±0.60 | 0.990 |
| ChCl:thioureab | 1170.9-1361.3 | 2409.4 | - 3.4017 | ±0.29 | 0.993 |

a313.15-363.15 K;b308.15-363.15 K

TABLE II. Parameters of Equation (2) in the temperature range of 293.15-363.15 K

| DES | c / kgm-3K-1 | α / K-1 | MRPD / % | R2 |
| --- | --- | --- | --- | --- |
| ChCl:propylene glycol | 7.2023 | 4∙10-4 | ±0.05 | 0.993 |
| ChCl:ethylene glycol | 7.1810 | 6∙10-4 | ±0.09 | 0.997 |
| ChCl:glycerol | 7.2629 | 6∙10-4 | ±0.02 | 0.990 |
| ChCl:urea | 7.1493 | 3∙10-4 | ±0.21 | 0.985 |
| ChCl:1,3-dimethylureaa | 8.7166 | 48∙10-4 | ±0.09 | 0.991 |
| ChCl:thioureab | 8.0453 | 27∙10-4 | ±0.06 | 0.991 |

a313.15-363.15 K;b308.15-363.15 K

TABLE III. The calculated values of Vm, Upot and Cp for the prepared DESs at 303.15 K

| DES | Vm / nm3 | Upot / kJmol-1 | Cp / Jmol-1 |
| --- | --- | --- | --- |
| ChCl:propylene glycol | 0.409 | 1156.7 | 469.8 |
| ChCl:ethylene glycol | 0.397 | 1169.8 | 457.5 |
| ChCl:glycerol | 0.451 | 1113.8 | 513.5 |
| ChCl:urea | 0.365 | 1208.0 | 424.4 |
| ChCl:1,3-dimethylureaa | 0.385 | 1184.7 | 444.1 |
| ChCl:thioureab | 0.356 | 1220.6 | 414.2 |

a313.15 K;b308.15 K

TABLE IV. Arrhenius equations for viscosity of the DESs studied over the temperature range 293.15-363.15 K

| DES | Viscosity range / Pas | Viscosity Arrhenius Equations (η / Pas) | Aη / Pas | Eη / Jmol-1 | MRPD/ % | R² |
| --- | --- | --- | --- | --- | --- | --- |
| ChCl:propylene glycol | 0.021-0.159 | ln η = 2984.7∙(T-1) - 12.2 | 5.14∙10-6 | 24815 | ±3.45 | 0.966 |
| ChCl:ethylene glycol | 0.007-0.059 | ln η = 2736.8∙(T-1) - 12.2 | 5.23∙10-6 | 22754 | ±2.10 | 0.963 |
| ChCl:glycerol | 0.008-0.490 | ln η = 6376.3∙(T-1) - 22.3 | 2.16∙10-10 | 53013 | ±8.13 | 0.983 |
| ChCl:urea | 0.018-3.195 | ln η = 8987.6∙(T-1) - 29.0 | 2.58∙10-13 | 74723 | ±19.72 | 0.968 |
| ChCl:1,3-dimethylureaa | 0.029-4.029 | ln η = 11489∙(T-1) - 35.5 | 4.01∙10-16 | 95519.5 | ±15.82 | 0.991 |
| ChCl:thioureab | 0.094-2.972 | ln η = 6971.9∙(T-1) - 21.7 | 3.88∙10-10 | 57964.4 | ±14.44 | 0.984 |

a313.15-363.15 K;b308.15-363.15 K

TABLE V. The adjustable parameters of VTF equation parameters of viscosity over the temperature range 293.15-363.15 K

| DES | VTF equation | η0 / Pas | Bη / K | T0 / K | MRPD / % | R² |
| --- | --- | --- | --- | --- | --- | --- |
| ChCl:propylene glycol | ln η = 252.03∙(T-T0)-1 - 5.7 | 3.348∙10-3 | 252.03 | 228 | ±1.61 | 0.990 |
| ChCl:ethylene glycol | ln η = 2636.3∙(T-T0)-1 - 12.01 | 6.107∙10-6 | 2636.3 | 6 | ±2.10 | 0.964 |
| ChCl:glycerol | ln η = 5393∙(T-T0)-1 - 20.68 | 1.044∙10-9 | 5393.0 | 26 | ±8.42 | 0.983 |
| ChCl:urea | ln η = 7400.3∙(T-T0)-1 - 26.43 | 3.32∙10-12 | 7400.3 | 30 | ±20.16 | 0.968 |
| ChCl:1,3-dimethylureaa | ln η = 4578.7∙(T-T0)-1 - 22.91 | 1.127∙10-10 | 4578.7 | 124 | ±9.57 | 0.995 |
| ChCl:thioureab | ln η = 2819.4∙(T-T0)-1 - 14.07 | 7.753∙10-7 | 2819.4 | 121 | ±18.73 | 0.984 |

a313.15-363.15 K;b308.15-363.15 K

TABLE VI. The thermodynamic functions of activation of viscous flow, as well as the values of ΔH*, ΔS* and ΔG* at 313.15 K, for the tested DESs

| DES | Eyring’s Equation | R2 | ∆H* / kJmol-1 | T∆S* / kJmol-1 | ∆G* / kJmol-1 |
| --- | --- | --- | --- | --- | --- |
| ChCl:propylene glycol | ln (ηV/hNA) = 2941.0∙T-1 + 1.3 | 0.965 | 24.5 | - 3.4 | 27.9 |
| ChCl:ethylene glycol | ln (ηV/hNA) = 2675.2∙T-1 + 1.3 | 0.962 | 22.2 | - 3.5 | 25.7 |
| ChCl:glycerol | ln (ηV/hNA) = 6311.7∙T-1 - 8.6 | 0.983 | 52.5 | 22.4 | 30.1 |
| ChCl:urea | ln (η∙V/h∙NA) = 8960.4∙T-1 - 15.7 | 0.968 | 74.5 | 40.8 | 33.7 |
| ChCl:1,3-dimethylurea | ln (ηV/hNA) = 10944∙T-1 - 20.4 | 0.989 | 91.0 | 53.2 | 37.8 |
| ChCl:thiourea | ln (ηV/hNA) = 6673.2∙T-1 - 7.5 | 0.983 | 55.5 | 19.5 | 36.0 |

TABLE VII. Arrhenius equations for conductivity with calculated pre-exponential factors and activation energies for DESs over the temperature range 293.15-363.15 K

| DES | Conductivity range / Sm-1 | Conductivity Arrhenius equations (κ /Sm-1) | Aκ / Sm-1 | Eκ / Jmol-1 | MRPD / % | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| ChCl:propylene glycol | 2.860-10.870 | ln κ = - 1948.6∙T-1 + 7.8 | 2584 | 16200 | ±4.72 | 0.957 |
| ChCl:ethylene glycol | 8.260-21.550 | ln κ = - 1391.4∙T-1 + 6.9 | 1012 | 11568 | ±0.95 | 0.989 |
| ChCl:glycerol | 1.088-11.227 | ln κ = - 3590.8∙T-1 + 12.3 | 220356 | 29853 | ±7.50 | 0.995 |
| ChCl:urea | 0.369-8.220 | ln κ = - 4574.1∙T-1 + 14.8 | 2808047 | 38029 | ±13.68 | 0.976 |
| ChCl:1,3-dimethylureaa | 0.264-1.119 | ln κ = - 3307.8∙T-1 + 9.2 | 10055.7 | 27501 | ±3.13 | 0.998 |
| ChCl:thioureab | 1.204-3.612 | ln κ = - 2240.5∙T-1 + 7.4 | 1718.1 | 18627.5 | ±1.83 | 0.999 |

a313.15-363.15 K;b308.15-363.15 K

TABLE VIII. VTF equation parameters of conductivity

| DES | VTF equation | κ0 / Sm-1 | Bκ / K | T0 / K | MRPD / % | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| ChCl:propylene glycol | ln κ = -98.52∙(T-T0)-1 + 3.2381 | 25.5 | 98.52 | 248.1 | ±0.34 | 0.999 |
| ChCl:ethylene glycol | ln κ = -196.76∙(T-T0)-1 + 4.2603 | 70.83 | 196.76 | 201.0 | ±0.75 | 0.994 |
| ChCl:glycerol | ln κ = -3375.5∙(T-T0)-1 + 11.968 | 157629.1 | 3375.5 | 9.9 | ±7.81 | 0.995 |
| ChCl:urea | ln κ = -601.12∙(T-T0)-1 + 5.9321 | 376.9 | 601.12 | 205.7 | ±4.27 | 0.996 |
| ChCl:1,3-dimethylureaa | ln κ = -527.38∙(T-T0)-1 + 3.3153 | 27.5 | 527.38 | 201.0 | ±11.63 | 0.992 |
| ChCl:thioureab | ln κ = -1086.9∙(T-T0)-1 + 5.4118 | 224.03 | 1086.9 | 100.8 | ±3.07 | 0.998 |

a313.15-363.15 K;b308.15-363.15 K

TABLE IX. VTF equation parameters of molar conductivity

| DES | VTF equation | (0 / Sm2mol-1 | B( / K | T0 / K | MRPD / % | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| ChCl:propylene glycol | ln Λ = -94.693∙(T-T0)-1 - 5.074 | 0.0063 | 94.693 | 250 | ±0.13 | 0.999 |
| ChCl:ethylene glycol | ln Λ = -280.42∙(T-T0)-1 - 3.710 | 0.0245 | 280.42 | 181 | ±0.31 | 0.995 |
| ChCl:glycerol | ln Λ = -3218.4∙(T-T0)-1 + 3.617 | 37.237 | 3218.4 | 20 | ±0.52 | 0.995 |
| ChCl:urea | ln Λ = -370.84∙(T-T0)-1 - 3.567 | 0.0282 | 370.84 | 230 | ±0.59 | 0.998 |
| ChCl:1,3-dimethylureaa | ln Λ = -3408.2∙(T-T0)-1 + 1.905 | 6.7212 | 3408.2 | 20 | ±0.16 | 0.999 |
| ChCl:thioureab | ln Λ = -2243.1∙(T-T0)-1 - 0.491 | 0.6122 | 2243.1 | 20 | ±0.17 | 0.999 |

a313.15-363.15 K;b308.15-363.15 K

TABLE X. Walden equation coefficients with MRPD and R2 for the DESs over the temperature range 293.15-363.15 K

| DES | α` | C | MRPD / % | R2 |
| --- | --- | --- | --- | --- |
| ChCl:propylene glycola | 66.54∙10-2 | 2.18∙10-4 | ±0.64 | 0.987 |
| ChCl:ethylene glycolb | 51.21∙10-2 | 5.00∙10-4 | ±0.96 | 0.956 |
| ChCl:glycerolc | 56.81∙10-2 | 2.17∙10-4 | ±0.73 | 0.994 |
| ChCl:uread | 48.91∙10-2 | 2.51∙10-4 | ±3.02 | 0.920 |
| ChCl:1,3-dimethylureae | 33.18∙10-2 | 0.92∙10-4 | ±0.68 | 0.987 |
| ChCl:thioureaf | 35.84∙10-2 | 3.63∙10-4 | ±0.68 | 0.983 |

alog (  = 0.6654∙log η-1 - 3.6612; blog (  = 0.5121∙log η-1 - 3.3006; clog (  = 0.5681∙log η-1 - 3.6631; dlog (  = 0.4891∙log η-1 - 3.5997; elog (  = 0.3318∙log η-1 - 4.0384 and flog (  = 0.3584∙log η-1 - 3.4401

TABLE XI. Parameters of the nD equation for the tested DESs in the range 293.15-363.15 K

| DES | nD range | Intercept | Slope | MRPD / % | R2 |
| --- | --- | --- | --- | --- | --- |
| ChCl:propylene glycol | 1.438-1.459 | 1.547 | - 0.0003 | ±4.10 | 0.994 |
| ChCl:ethylene glycol | 1.467-1.488 | 1.576 | - 0.0003 | ±3.99 | 0.999 |
| ChCl:glycerol | 1.472-1.486 | 1.545 | - 0.0002 | ±2.71 | 0.997 |
| ChCl:ureaa | 1.493-1.507 | 1.566 | - 0.0002 | ±2.67 | 0.997 |
| ChCl:1,3-dimethylureaa | 1.469-1.480 | 1.5338 | - 0.0002 | ±0.46 | 0.977 |
| ChCl:thioureab | 1.509-1.525 | 1.6019 | - 0.0003 | ±0.89 | 0.974 |

aTemperature range: 303.15-363.15 K, *298.15-363.15 K

TABLE XII. The phase velocity (υ) and the molar refractivity (A) for the prepared DESs in the temperature range of 293.15-363.15 K

| DES | υ / ms-1∙107 | A / m3mol-1∙10-6 |
| --- | --- | --- |
| ChCl:propylene glycol | 20.56-20.86 | 66.30-67.02 |
| ChCl:ethylene glycol | 20.15-20.44 | 68.62-68.89 |
| ChCl:glycerol | 20.18-20.37 | 77.85-79.09 |
| ChCl:urea | 19.90-20.09 | 65.06-65.39 |
| ChCl:1,3-dimethylureaa | 20.26-20.41a | 65.64-83.00b |
| ChCl:thioureab | 19.66-19.87a | 66.11-74.45b |

a298.15-363.15 K, b313.15-363.15 K

# Footnotes

( Vlada B. Veljković, Faculty of Technology, University of Niš, Bulevar Oslobođenja 124, 16000 Leskovac, Serbia, e-mail: veljkovicvb@yahoo.com