Supplementary material

Arsenic removal from water using a one-pot synthesized low cost mesoporous

Fe-Mn modified biosorbent

Jasmina Nikić1, Malcolm Watson1, Aleksandra Tubić1, Marijana Kragulj Isakovski1, Snežana Maletić1, Emilijan Mohora2 and

Jasmina Agbaba1*

1 University of Novi Sad, Faculty of Sciences, Department of Chemistry, Biochemistry and Environmental Protection, Trg Dositeja Obradovića 3, 21000 Novi Sad, Serbia; 2 Singidunum University, Faculty of applied ecology Futura, Požeška 83a, 11 030 Beograd, Serbia

Figure S1. SEM images of Chit and Chit-FeMn

Figure S2. EDS analysis graph of Chit and Chit-FeMn

Figure S3. XRD patterns of Chit and Chit-FeMn

Figure S4. Effect of NOM on As(III) and As(V) removal by Chit-FeMn. Initial As concentration 0.5 mg L-1, sorbent dose 0.5 g L-1, pH = 7.0±0.2

TABLE SI. Diffusion parameters for adsorption of As(III) and As(V) onto Chit and Chit-FeMn

|  | Intra particle diffusion parameters |  |  |  |
| --- | --- | --- | --- | --- |
|  | Ki / µg g-1 min-0,5 | Ci / µg g-1 | SSE | R2 |
|  | As(III) |  |  |  |
| Chit | a21.9 | 21.9 | 861 | 0.9826 |
|  | b0.756 | 249 | 40 | 0.4880 |
| Chit-FeMn | a30.7 | 25.0 | 481 | 0.9932 |
|  | b16.4 | 16.4 | 521 | 0.9794 |
|  | c5.70 | 5.70 | 3.23 | 0.9918 |
|  | As(V) |  |  |  |
| Chit | a9.94 | 427 | 477 | 0.9744 |
|  | b0.206 | 617 | 17.9 | 0.9742 |
| Chit-FeMn | a46.1 | 134 | 2030 | 0.9656 |
|  | b10.1 | 518 | 309 | 0.9681 |
|  | c3.64 | 682 | 3.82 | 0.9938 |

aFirst, bsecond and cthird linear regions.

TABLE SII. Characteristics of the contaminated groundwater

| Parameter |  | Unit |
| --- | --- | --- |
| pH | 8.27 |  |
| Conductivity | 727 | µS cm-1 |
| Hardness | 165 | mg L-1 |
| As | 35 | µg L-1 |
| Fe | 0.213 | mg L-1 |
| Mn | 0.016 | mg L-1 |
| Phosphate | 0.391 | mg L-1 |
| Sulfate | 41.02 | mg L-1 |
| Nitrate | 0.169 | mg L-1 |
| Chloride | 6.12 | mg L-1 |
| DOC | 5.54 | mg L-1 |
| UV | 0.209 | cm-1 |

*Corresponding author. E-mail: jasmina.agbaba@dh.uns.ac.rs