Supplementary material

Influence of various cosolvents on the calcium oxide-catalyzed sunflower oil ethanolysis

DUŠICA R. ĐOKIĆ-STOJANOVIĆ1, ZORAN B. TODOROVIĆ2, DRAGAN Z. TROTER2*, OLIVERA S. STAMENKOVIĆ2 and VLADA B. VELJKOVIĆ2

1Zdravlje Actavis, Vlajkova 199, 16000 Leskovac, Serbia and  2Faculty of Technology, University of Niš, Bulevar Oslobođenja 124, 16000 Leskovac, Serbia

* Corresponding author. E-mail: drtroter@gmail.com

TABLE S-I. The properties of the employed cosolvents and ethanol

| Cosolvent* | TEOA | DEOA | EG | MEK | HEX | TEA | Glyme | GLYC | THF | DIOX | ET |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Chemical formula | C6H15NO3 | C4H11NO2 | C2H6O2 | C4H8O | C6H14 | C6H15N | C4H10O2 | C3H8O3 | C4H8O | C4H8O2 | C2H6O |
| Boiling point (°C)** | 335.0 | 268.0 | 197.6 | 79.6 | 68.0 | 89.7 | 83.5 | 290.0 | 65.0 | 101.1 | 78.5 |
| Melting point (°C)** | 21.5 | 28.0 | -13.0 | -86.0 | -95.0 | -115.0 | -58.0 | 19.0 | -108.3 | 11.8 | -114.1 |
| Density (g/cm3) |  |  |  |  |  |  |  |  |  |  |  |
| at 25°C | 1.12b | – | 1.11b | 0.799b | 0.656b | 0.724b | 0.865b | 1.257b | 0.88b | 1.029b | 0.787b |
| at 20°C | 1.1242c,e | 1.0966c,e | 1.1088c,e | 0.8054c | 0.6593e | 0.7275c | 0.8691c | 1.261c | 0.8892c | 1.0337c | 0.7893c |
| Viscosity at 25°C (mPas) | 652.576b; 609c | 109.5 (at 50 °C) | 17.645b; 16.1c | 0.396b; 0.405c | 0.296b; 0.300c | 0.341b; 0.347c | 0.446b | 749.3b; 934c | 0.465b; 0.456c | 1.211b; 1.177c | 1.057b; 1.074c |
| Partition coefficients at 25°C (logP) | - 1.00b; - 1.59e; - 2.3f | - 1.43 (20 °C)b,e | - 1.36b,e | 0.29a,b,c,e,f | 3.90b,e; 4.0a,c,f | 1.45 a,b,c; 1.64e | - 0.21b | - 1.76b | 0.46 (20 °C)a | - 0.27b,e; - 0.49f | - 0.31b,e; - 0.30a,c |
| Refractive index at 25°C | 1.4835b | 1.4747 (19 °C)b | 1.4306b | 1.3764b | 1.3723b | 1.3980b | 1.3781b; 1.3770c | 1.4730b | 1.405b,c | 1.4202b | 1.3594b |
| Dipole moment, D | 3.57c,d; 3.48f | 0.85b; 2.8c | 2.31b; 2.36c; 2.28c | 2.76b; 2.779c; 2.78f | 0.00b; 0.08f | 0.66b,c | 1.71b | 4.21b; 2.56c | 1.63b,f; 1.75c; | 0.00b,c; 0.45f | 1.69b,c |
| Dielectric constant (20 °C) | 29.36 (25 °C)c,d | 25.75c | 41.4c | 18.56c | 1.8865c | 2.418c | 7.30 (23.7 °C)c | 46.53c | 7.52c (22.2 °C) | 2.2189c | 25.3c |

*TEOA - triethanolamine, DEOA - diethanolamine, EG - ethylene glycol, MEK - methyl ethyl ketone, HEX - n-hexane, TEA - triethylamine, Glyme - ethylene glycol dimethyl ether, GLYC - glycerol, THF - tetrahydrofuran, DIOX - dioxane and ET - ethanol.**According to Material Safety Data Sheet. aref [1]; bref [2]; cref [3]; dref [4]; eref [5]; fref [6].

REFERENCES

- J. Sangster, J. Phys. Chem. Ref. Data 18 (1989) 1111 (https://doi.org/10.1063/1.555833)

- C. L.Yaws, Chemical properties handbook: physical, thermodynamic, environmental, transport, safety, and health related properties for organic and inorganic chemicals, McGraw-Hill, New York, USA, 1999

- D. R. Lide, CRC Handbook of Chemistry and Physics, 84th ed., CRC Press LLC; 2003

- J. A. Dean, Lange's handbook of chemistry, 15th ed., McGraw-Hill, New York, USA, 1999

- D. Mackay, W. Y. Shiu, K.-C. Ma, S. C. Lee, Handbook of physical-chemical properties and environmental fate for organic chemicals, 2nd ed., CRC Press, Boca Raton, USA, 2006

- Z. B. Todorović, O. S. Stamenković, I. S. Stamenković, J. M. Avramović, A. V. Veličković, I. B. Banković-Ilić, V. B. Veljković, Fuel 107 (2013) 493 (https://doi.org/10.1016/j.fuel.2012.11.049)

# Footnotes

* Dragan Z. Troter. E-mail: drtroter@gmail.com