Supplementary material

Towards edible ionic liquids – cholinium taurate

MILAN VRANEŠ*, ALEKSANDAR TOT, JOVANA PANIĆ, SNEŽANA PAPOVIĆ, SLOBODAN GADŽURIĆ and DRAGANA ČETOJEVIĆ-SIMIN1

Faculty of Sciences, Department of Chemistry, Biochemistry and Environmental Protection, University of Novi Sad, Trg Dositeja Obradovića 3, 21000 Novi Sad, Serbia

1 Oncology Institute of Vojvodina, Institutski Put 4, 21204 Sremska Kamenica, Serbia

Figure S1. 1H NMR and 13C NMR spectra of [Chol][Tau]

Figure S2. FTIR spectrum of [Chol][Tau]

Table S1. Viscosity, and density and thermal expansion coefficient values of [Chol][Tau]

in the temperature range from (20 to 50) ºC

| T / (ºC) | η / (mPa·s) | d / (g·cm–3) | αp⸱104 / (K–1) |
| --- | --- | --- | --- |
| 20 | 1434.53 | 1.23140 | 5.08 |
| 25 | 985.12 | 1.22845 | 5.09 |
| 30 | 691.54 | 1.22538 | 5.10 |
| 35 | 503.78 | 1.22225 | 5.12 |
| 40 | 374.72 | 1.21911 | 5.13 |
| 45 | 284.91 | 1.21591 | 5.14 |
| 50 | 224.12 | 1.21266 | 5.16 |

# Footnotes

*Corresponding author. E-mail: milan.vranes@dh.uns.ac.rs