June 25th 2019

Editor-in-Chief

Journal of the Serbian Chemical Society

Dear Professor Branislav Z. Nikolic,

Re: Submission of a research manuscript for consideration of publication in the Journal of the Serbian Chemical Society

A manuscript entitled “Porous Amphiphilic Biogel from Facile Chemo-Biosynthetic Route” is submitted online to the journal for publication consideration. The manuscript is submitted as a full-length research article.

2. Mandatory declaration

All of the authors for the manuscript agreed to submit the work to the journal. All of the authors certified that the work has not been published or submitted or being submitted to another journal. The authors declare that the submission is the original work of the authors and it has never been submitted before to Journal of the Serbian Chemical Society. The authors also declare no conflict of interests.

3. Suggestion for an abbreviated running title: “Radical grafting of mcl-PHA”.

4. Lay Abstract:

Background: Whilst mcl-PHA has attracted great interest in research due to its potential wide applicability as biomaterials, its strong hydrophobicity, slow degradation under physiological conditions and lack chemical functionalities hinder the realization of its potentials.

Findings: Glycerol 1,3-diglycerolate diacrylate (GDD) was graft copolymerized onto poly(3-hydroxyoctanoate-co-3-hydroxyhexanoate) P(3HO-co-3HHX) to render the latter more hydrophilic. Grafting of P(3HO-co-3HHX) backbone was performed using benzoyl peroxide as free radical initiator in homogenous acetone solution. Radical-mediated grafting generated (-( carbon inter-linking of mcl-PHA and GDD resulted in macromolecular structure with gel properties. Different parameters affecting the graft yield viz. monomer concentration, initiator concentration, temperature and reaction time were also investigated. A detail mechanism scheme provides significant improvement to previous literature.

Impacts: Functionalization of mcl-PHA by introducing elements of hydrophilicity has been shown to improve its cellular interaction behaviour. Innovative niche applications from its uses as platform material will also be made possible e.g. in devising drug delivery vehicles, nano-emulsion preparation, biomedical scaffolds, bio-anode in microbial fuel cell amongst others. Thus, radical-mediated grafting of mcl-PHA produced from bacterial fermentation to yield functionalized bioplymer, as shown in this study, adds to the available repertoire of functional materials for such purposes.

5. The corresponding author for this manuscript is:

Dr. M. Suffian M. Annuar,

Institute of Biological Sciences

Faculty of Science

University of Malaya

Kuala Lumpur 50603

MALAYSIA

Tel: 6-03-7967-7182

Fax: 6-03-7967-4178

E-mail: suffian_annuar@um.edu.my

6. The co-authors for the manuscript are:

(a) Syed Mohammad Daniel Syed Mohamed

Institute of Biological Sciences

Faculty of Science

University of Malaya

Kuala Lumpur 50603

Malaysia

Email: syed_daniel@um.edu.my

(b) Dr. Thorsten Heidelberg

Department of Chemistry

Faculty of Science

University of Malaya

Kuala Lumpur 50603

Malaysia

Email: heidelberg@um.edu.my

(c) Dr. Nor Faezah Ansari

Department of Biotechnology,

Kulliyyah of Science, International Islamic University Malaysia,

Bandar Indera Mahkota 25200 Kuantan, Pahang, Malaysia

Email: faezahansari@iium.edu.my

(d) Nor Hidayah Ismail

Research Cluster Office,

Institute of Research Management and Services,

University of Malaya, 50603 Kuala Lumpur, Malaysia

Email: nor_hidayah@um.edu.my

We look forward to hearing favorable news from you.

Thank you.

Yours truly,

M. Suffian M. Annuar, Ph.D

POTENTIAL REVIEWERS

| 1. PROFESSOR DR. MANFRED ZINN |
| --- |
| University of Applied Sciences Western Switzerland (HES-SO) Institute for Life Technologies Route du Rawyl 47 CH-1950 Sion, Switzerland |
| Email | : | manfred.zinn@hevs.ch |

| 2. PROFESSOR DR. BAKI HAZER |
| --- |
| Bülent Ecevit University, College of Arts and Science, Department of Chemistry, 67100 Zonguldak, Turkey |
| Email | : | bkhazer@karaelmas.edu.tr |

- PROFESSOR DR. TAKEHARU TSUGE,

Department of Innovative and Engineered Materials,

Tokyo Institute of Technology,

J2-47, 4259 Nagatsuta, Midori-ku, Yokohama 226-8502, Japan

E-mail: tsuge.t.aa@m.titech.ac.jp