Modeling of chlorinated phenols adsorption on polyethylene and polyethylene terephtalate microplastic

LONČARSKI MAJA1, TUBIĆ ALEKSANDRA*,1, KRAGULJ ISAKOVSKI MARIJANA1, JOVIĆ BRANISLAV1, APOSTOLOVIĆ TAMARA1, NIKIĆ JASMINA1,

AGBABA JASMINA1

Supplementary material

Table S1. Physico-chemical properties of the investigated chlorophenols

| Compounds | MW, g mol-1 | log Kowa | Via / cm3 mol-1 10-2 | Swa / mg l-1 | pKaa |
| --- | --- | --- | --- | --- | --- |
| 4-CP | 129 | 2.40 | 1.02 | 27100 | 8.85 |
| 2,4-DCP | 163 | 3.06 | 1.14 | 4500 | 7.90 |
| 2,4,6-TCP | 197 | 3.69 | 1.26 | 800 | 6.40 |
| PCP | 266 | 5.12 | 1.39 | 14 | 4.80 |

MW - molecular weight; Kow, octanol-water partition coefficient; Vi - McGowan volume. aKragulj et al.

Analytical procedure, quality assurance and quality control

Chlorinated phenol concentrations were determined by gas chromatography with mass spectrometry detection (GC/MSD), requiring an acetylating step prior to analysis. For acetylation of chlorinated phenols, K2CO3 and acetanhydride was added to the aqueous solution and stirred for 15 min to ensure complete acetylation of the phenols. The acetylated phenols were extracted using hexane (J.T. Baker, for organic residue analysis) with 15 min of shaking. The acetylated phenols were analyzed by Agilent 7890A/5975C GC/MSD on a HP-5MS column (J&W Scientific) using the following conditions: helium carrier gas at a flow rate of 1.5 ml/min in the column; injector temperature 200 ºC; initial oven temperature 40 ºC for 2 min, then 40 ºC/min to 100ºC for 0.5 min, then 2 ºC/min to 140 ºC and 30 ºC/min to 300 ºC; detector temperature 150 ºC. The sample volume injected was 2 µl. Blank and control experiments were performed in parallel to the sorption experiments. Blank tests, containing same amounts of background solution and solid particles as the samples, but without the addition of chlorinated phenols, were carried out using conditions similar to those described previously, and no target compound was found. Control tests were carried out in 20 mL of background solution containing a same gradient of CP concentrations as the samples, but without solid particles, in order to evaluate the loss of CP resulting from some additional removal processes, such as volatilization and/or sorption to the wall of glass bottles. Recovery of selected CP after derivatization with acetanhydride and liquid-liquid extraction with hexane ranged from 80-116 with the relative standard deviations (RSD) being below 10 % for all CPs. The method detection limits (MDLs) of the applied analytical methods ranged between 0.11-0.53 μg L-1. The correlation coefcient for the chlorinated phenols calibration curve was higher than 0.99. All the reported concentrations of CP were corrected with the recovery efficiency and internal standard.

a)

b)

c)

Fig.S1  Images of the microplastic particles used in experiments: a) PE, b)  PE_PCPs_1  and c)  PE_PCPs_2

Fig.S2 Kinetic study results of 4-CP, 2,4-DCP, 2,4,6-TCP and PCP on a) PE, b) PE_PCPs_1,

c) PE_PCPs_2 and d) PET (during 96 h, pH 6.8±0.5, initial CPs concentration 100µg L-1)

Fig. S3. Linear plots of sorption pseudo-second-order kinetic model for 2,4-DCP, 2,4,6-TCP and PCP onto a) PE, b) PE_PCPs_1, c) PE_PCPs_2 and d) PET

Fig S4. Linear plots of sorption modelled with intraparticle diffusion kinetics for 2,4-DCP, 2,4,6-TCP and PCP on a) PE, b) PE_PCPs_1, c) PE_PCPs_2 and d) PET

Table S2. Theoretical and experimental qe values obtained with pseudo-second-order model

| Compounds | Sorbents | k1 (h-1) | R2 | qe (theoretical) | qe (experimental) | SD |
| --- | --- | --- | --- | --- | --- | --- |
| 4-CP | PE | 0.0064 | 0.998 | 142.9 | 141.6 | 0.88 |
|  | PE_PCPs_1 | 0.0120 | 0.994 | 84.50 | 89.85 | 3.76 |
|  | PE_PCPs_2 | 0.0130 | 0.987 | 77.40 | 79.33 | 1.36 |
|  | PET | 0.0140 | 0.998 | 69.69 | 69.71 | 0.01 |
| 2,4-DCP | PE | 0.0045 | 0.999 | 222.2 | 223.2 | 0.66 |
|  | PE_PCPs_1 | 0.0054 | 0.995 | 188.7 | 189.6 | 0.69 |
|  | PE_PCPs_2 | 0.0044 | 0.992 | 223.7 | 226.1 | 1.68 |
|  | PET | 0.0080 | 0.998 | 126.3 | 125.6 | 0.44 |
| 2,4,6-TCP | PE | 0.0066 | 0.991 | 156.3 | 157.7 | 1.03 |
|  | PE_PCPs_1 | 0.0057 | 0.998 | 175.4 | 176.8 | 0.95 |
|  | PE_PCPs_2 | 0.0053 | 0.999 | 199.0 | 207.9 | 6.29 |
|  | PET | 0.0153 | 0.998 | 65.57 | 67.43 | 1.32 |
| PCP | PE | 0.0110 | 0.998 | 90.09 | 90.66 | 0.40 |
|  | PE_PCPs_1 | 0.0130 | 0.995 | 81.30 | 80.66 | 0.45 |
|  | PE_PCPs_2 | 0.0100 | 0.992 | 104.1 | 103.0 | 0.74 |
|  | PET | 0.0430 | 0.990 | 23.94 | 25.75 | 1.28 |

Table S3. Freundlich and Langmuir parameters for adsorption of CPs on MPs

| Compounds | Sorbents | Freundlich model |
| --- | --- | --- |
|  |  | R2 | n | KF / (µg g-1/µg l-1)n | log Kd |
|  |  |  |  |  | 0.01 Sw | 0.05 Sw | 0.5 Sw |
| 4-CP | PE | 0.967 | 0.60 | 4.02 | 1.51 | 1.18 | 0.95 |
|  | PE_PCPs_1 | 0.967 | 0.94 | 1.65 | 1.28 | 1.05 | 0.71 |
|  | PE_PCPs_2 | 0.982 | 0.75 | 3.88 | 1.29 | 1.02 | 0.63 |
|  | PET | 0.999 | 0.90 | 1.29 | 1.86 | 1.69 | 1.45 |
| 2,4-DCP | PE | 0.969 | 0.63 | 0.94 | 1.63 | 1.35 | 1.16 |
|  | PE_PCPs_1 | 0.985 | 0.58 | 3.45 | 1.59 | 1.30 | 0.86 |
|  | PE_PCPs_2 | 0.977 | 0.75 | 1.02 | 1.29 | 1.12 | 0.86 |
|  | PET | 0.971 | 0.92 | 0.29 | 2.10 | 2.05 | 1.96 |
| 2,4,6-TCP | PE | 0.947 | 0.66 | 1.39 | 1.82 | 1.58 | 1.24 |
|  | PE_PCPs_1 | 0.961 | 0.6 | 1.69 | 1.67 | 1.40 | 0.99 |
|  | PE_PCPs_2 | 0.99 | 0.6 | 1.50 | 1.61 | 1.32 | 0.92 |
|  | PET | 0.989 | 0.85 | 0.99 | 2.41 | 2.31 | 2.16 |
| PCP | PE | 0.959 | 0.57 | 1.78 | 2.34 | 2.04 | 1.61 |
|  | PE_PCPs_1 | 0.931 | 0.53 | 1.57 | 2.18 | 1.85 | 1.38 |
|  | PE_PCPs_2 | 0.945 | 0.54 | 0.63 | 1.81 | 1.49 | 1.02 |
|  | PET | 0.953 | 0.94 | 0.93 | 2.84 | 2.79 | 2.73 |
| Compounds | Sorbents | Langmuir model |
|  |  | R2 | qmax / µg g-1 | KL / l µg-1 | RL |
| 4-CP | PE | 0.997 | 63.30 | 0.0530 | 0.203-0.972 |
|  | PE_PCPs_1 | 0.974 | 282.9 | 0.0059 | 0.210-0.965 |
|  | PE_PCPs_2 | 0.967 | 86.90 | 0.0058 | 0.745-0.997 |
|  | PET | 0.999 | 335.5 | 0.0030 | 0.828-0.998 |
| 2,4-DCP | PE | 0.921 | 44.90 | 0.0066 | 0.624-0.996 |
|  | PE_PCPs_1 | 0.992 | 55.30 | 0.0339 | 0.267-0.986 |
|  | PE_PCPs_2 | 0.967 | 86.90 | 0.0058 | 0.668-0.996 |
|  | PET | 0.973 | 104.7 | 0.0023 | 0.826-0.998 |
| 2,4,6-TCP | PE | 0.984 | 22.90 | 0.0391 | 0.223-0.974 |
|  | PE_PCPs_1 | 0.974 | 38.70 | 0.0186 | 0.377-0.989 |
|  | PE_PCPs_2 | 0.993 | 27.80 | 0.0294 | 0.276-0.984 |
|  | PET | 0.990 | 198.4 | 0.0039 | 0.763-0.998 |
| PCP | PE | 0.949 | 15.60 | 0.1354 | 0.077-0.937 |
|  | PE_PCPs_1 | 0.948 | 23.70 | 0.0243 | 0.306-0.985 |
|  | PE_PCPs_2 | 0.939 | 7.70 | 0.0691 | 0.130-0.951 |
|  | PET | 0.956 | 309.9 | 0.0027 | 0.825-0.999 |