SUPPLEMENTARY MATERIAL TO

Fabrication of bionanocomposite based on LDH using biopolymer of gum arabic and chitosan-coating for sustained drug-release

MILAD ABNIKI, ALI MOGHIMI and FARIBORZ AZIZINEJAD

Department of Chemistry, Varamin-Pishva Branch, Islamic Azad University, Varamin, Iran

Fig. S-1. Molecular size and structure of MEF

Drug adsorption mechanism

In order to evaluate the mechanism of MEF adsorption, 0.02 g of LDH-Cl was placed in the ultrasonic apparatus for 30 min. Beakers containing a solution of the MEF were prepared at different concentrations of 0.5, 1, 2, 3, 4, 5, 7, 8, 9, 10 mg L-1 and then 0.02 g of LDH-Cl added to each beaker. The pH of mixtures was adjusted to 10 by buffer solution and stirred for 24 h at 25 °C. The absorbance of the solutions was recorded by the UV device at 285 nm. The equilibrium concentration (qe) of MEF adsorbed by LDH-Cl was calculated from the following equation:

(S-1)

Where qe is the equilibrium concentration (mg g-1), C0 and Ce are the initial concentration and concentration equilibrium (mg L-1) of MEF, respectively. V is the volume of experiment solution (L) and m is the amount of LDH-Cl (g).1

Drug adsorption isotherms

The adsorption isotherms of MEF by LDH-Cl were investigated based on Langmuir, Freundlich and Temkin models. The Langmuir adsorption isotherm is expressed according to the following equation, in which the adsorption relation is defined as single-layer and homogeneous.

(S-2)

In relation (S-2) qm is the maximum sorption of MEF per gram of LDH-Cl (mg g-1), and KL is Langmuir constant (L mg-1). Also, for obtaining the dimensionless factor, Another Langmuir's relation has been used:

(S-3)

In relation (S-3), RL is a dimensionless factor. The smaller value of RL indicates the optimal adsorption. RL can be obtained in four adsorption modes: (RL>1) which adsorption is undesirable, (RL=1) linearly, (0<RL<1) desirable, and (RL=0)  irreversible.

The Freundlich adsorption isotherm is expressed as a heterogeneous and multilayer adsorption and calculates from the following relation:

(S-4)

Where qe and ce are the same as defined in relation (S-1), KF is Freundlich constant (L g-1), n is adsorption intensity, (1/n) is the inhomogeneous factor and expressed in three ways depending on its value: (1/n>1) adsorption is undesirable,(1/n=0) adsorption is irreversible, (0<1/n<1) adsorption is desirable.2

The Temkin isotherm suggests the sorption energy decreases linearly when increasing the sites occupied by molecules.

(S-5)

(S-6)

In relation (S-5) qe and Ce are the same as defined in relation (S-1), R is gas constant (8.314 J mol-1 K-1), T is temperature (K), b is the Temkin isotherm constant, A is the Temkin binding equilibrium constant (L g-1 ), B is a constant and is an index of sorption heat (J mol-1).

## Adsorption isotherms

In this study, three isotherm models were investigated to explain the relationship between adsorbate (MEF) and adsorbent (LDH). Fig. S-2 shows the isotherm curves of MEF adsorption. The results of adsorption isotherms are listed in Table S-I, indicate that the data ﬁtted good in the Langmuir model with coefﬁcient value (R2 = 0.95). This result of the Langmuir model confirms that MEF molecules are homogeneously intercalated in the interlayer space of LDH. The qmax and KL obtained from the Langmuir model were 2.17 mg g-1 and 0.55 L mg-1, respectively at 25 °C. These two parameters show the maximum LDH capacity in the MEF adsorption.3 Also, the separation factor (RL) achieved from Langmuir isotherm was 0.78, indicating that the adsorption of MEF by LDH is favorable.4 Furthermore, with respect to the value of R2 = 0.94 for Freundlich isotherm, the next step of MEF adsorption carried out on the surface of the LDH.5

Fig. S-2. The isotherm curves of MEF adsorption by LDH-Cl at 25 ºC (A Langmuir, B Freundlich, and C Temkin)

TABLE S-I. Isotherms parameters of MEF adsorption

| Langmuir isotherm parameters | Freundlich isotherm parameters |  | Temkin isotherm parameters |  |
| --- | --- | --- | --- | --- |
| qmax / mg g-1 |  | 2.17 |  | Kf / L g-1 | 0.69 |  | A / L g-1 | 9.6 |  |
| KL / L mg-1 |  | 0.55 |  | n | 1.9 |  | B / J mol-1 | 0.39 |  |  |
| RL |  | 0.78 |  | R2 | 0.94 |  | R2 | 0.93 |  |  |
| R2 |  | 0.95 |  |  |  |  |  |  |  |  |

Investigation of adsorption kinetics

In this research, the mechanisms of adsorption kinetic of MEF by LDH-Cl were investigated. In this way, several beakers containing 100 mL of 5 mg L-1 MEF solution at pH=10 were stirred at different intervals and constant speed at 25 °C. The amount of MEF in the solutions after a certain time period was reported by UV-VIS spectrometry at 285 nm. Then, the pseudo-first-order and pseudo-second-order mechanisms were studied for kinetic adsorption of MEF by LDH-Cl.

(S-7)

In the above equation qe is the amount of adsorption in equilibrium, qt is the amount of adsorption at t / min with per unit (mg g-1), and k1 is the pseudo-first-order rate constant (min-1).6 The second-order adsorption mechanism is as follows:

(S-8)

In the above relation, qe and qt are the same as defined in relation (S-7), and k2 is the pseudo-second-order rate constant (g mg-1 min-1).4

In Fig. S-3 are presented the curves of the kinetics of MEF sorption. According to the results deposited in Table S-II, the sorption of MEF follows from the pseudo-second-order adsorption kinetics corresponds to R2=0.999. A good accord is seen between the qex (experimental adsorption capacity) and the qe (calculated adsorption capacity) attained from the pseudo-second kinetic model. Additionally, the value of the rate constant for pseudo-first-order kinetics achieved a very small amount (k1 = 0.003), which indicates the high rate of MEF adsorption by LDH.

Fig. S-3. The pseudo-first-order adsorption kinetics (A) and pseudo-second-order adsorption kinetics (B) of MEF

TABLE S-II. The parameters of the pseudo-first-order kinetics and pseudo-second-order kinetics of MEF adsorption

| qex / mg g-1 | 1.38 | Pseudo-first order kinetics parameters |  | Pseudo-second order kinetics parameters |  |
| --- | --- | --- | --- | --- | --- |
|  |  | qe / mg g-1 | 0.50 |  |  | qe / mg g-1 | 1.39 |  |  |
|  |  | k1 / min-1 | 0.003 |  |  | k2 / g mg-1 min-1 | 0.04 |  |  |
|  |  | R2 | 0.85 |  |  | R2 | 0.99 |  |  |

Determination of MEF loading

A quantity of 0.2 g of LDH-MEF, LDH-MEF/CHIT, or LDH-MEF/GUM/CHIT was dispersed in 50 mL of phosphate buffer (pH=7.4) and was stirred at 100 rpm for 12 h. After that, the pH of the suspension was adjusted to 1.2 using 1 M hydrochloric acid solution and then by keeping the conditions the stirring was continued for 12 h. The solution was centrifuged, and its absorption was recorded at 285 nm. All steps were repeated three times in identical conditions and the encapsulation efficiency was calculated according to the following equation7:

(S-9)

Encapsulation efﬁciency

In this study, the amount of drug encapsulation in three carriers was determined and shown in Table S-III. As is displayed in Table S-III, the encapsulation efficiency of MEF shows a dependence on carrier formulation. By co-intercalation of MEF/GUM into the LDH, an increase in the encapsulation efficiency of MEF is observed, which is due to the formation of an amphiphilic emulsion of GUM that allows the retention of more MEF molecules during the hybrid preparation.8 Therefore, this formulation loaded with co-intercalation of MEF/GUM into the LDH exhibits higher encapsulation efficiency.

TABLE S-III. Encapsulation efﬁciency of MEF

| Composition | Encapsulation efficiency, % |
| --- | --- |
| LDH-MEF | 31.23 ±0.57 |
| LDH-MEF/CHIT | 30.01 ±0.61 |
| LDH-MEF/GUM/CHIT | 44.12 ±0.74 |

## In vitro release of MEF

The release of MEF from LDH-MEF, LDH-MEF/CHIT, and LDH-MEF/GUM/CHIT was performed into a simulated environment at pH=1.2 (0.1 M HCl) and pH=7.4 (0.1 M phosphate buffer) at 37 ºC. The test environment consisted of one beaker of 50 mL of the desired buffer and 0.2 g carrier, then these suspensions were stirred at 50 rpm for 60 min (pH=1.2) and 660 min for (pH=7.4).9 The sampling was carried out at definite intervals, and then the concentration of MEF released in the medium was analyzed by the UV spectrophotometer at 285 nm.

## Optimization of pH and loading time

This research studied the LDH-Cl with a liquid solution of MEF at pH values of 5-12 as shown in Fig. S-4. The optimum pH value for MEF adsorption was 10. This is due to the formation of mefenamate anion at pH=10 and the structure of the LDH which has a high positive charge of the layers for anionic exchange of chloride anions in the interlayer by MEF anions at pH values of higher than 10. The loading time of MEF adsorption at pH=10 optimized and indicating that the high percentage of MEF is sorbed in a time interval. As shown in Fig. S-5, the LDH-Cl adsorbed 70 % of MEF within the first 100 min which can be related to surface adsorption and intercalation within the interlayer space.

Fig. S-4. Sorption of MEF using LDH-Cl at diﬀerent pH. The volume of each solution (10 mL) containing 5 μg mL-1 of MEF. The pH values of solutions were adjusted to 5 to12 by buﬀer solutions. The 0.02 g of LDH-Cl was dispersed to each solution and the suspension was stirred for 24 h

Fig. S-5. Effect of time on percentage sorption of MEF by LDH-Cl at pH=10. The volume of each solution (10 mL) containing 5 μg mL-1 of MEF at pH=10. The 0.02 g of LDH-Cl was dispersed to each solution and the suspension was stirred for different length of time

Release kinetics of MEF

The release data of two buffer solutions (1.2 and 7.4) were ﬁtted to by various kinetic models in order to comprehend the dynamics of MEF release from LDH samples. Different kinetic models (Korsmeyer–Peppas, zero and ﬁrst order model) were applied to ﬁt the MEF release data using the KinetDS v3.0 software.4,10 MEF release from LDH-MEF, LDH-MEF/CHIT, and LDH-MEF/GUM/CHIT at 1.2 and 7.4 follow Korsmeyer–Peppas pattern with good ﬁtting coeﬃcients (TABLE S-IV). Based on the value of release exponent (n) for LDH samples at 1.2 and 7.4, the release of MEF from all samples follows non-Fickian transport mechanism.

TABLE S-IV. Kinetic models of the MEF release from the LDH samples in two buffer solutions

| Buﬀer solution | Sample | Zero-order |  | First-order |  | Korsmeyer-Peppas |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | R2 | R2 |  | R2 | n |
| 1.2 | LDH-MEF | 0.7151 | 0.2457 |  | 0.9967 | 0.757 |
|  | LDH-MEF/CHIT | 0.9227 | 0.2716 |  | 0.9996 | 0.744 |
|  | LDH-MEF/GUM/CHIT | 0.9225 | 0.3027 |  | 0.9976 | 0.725 |
| 7.4 | LDH-MEF | 0.5716 | 0.2658 |  | 0.9960 | 0.698 |
|  | LDH-MEF/CHIT | 0.6978 | 0.3023 |  | 0.9985 | 0.687 |
|  | LDH-MEF/GUM/CHIT | 0.9006 | 0.3563 |  | 0.9967 | 0.675 |

REFERENCES

1.	D. Ž. Ivetić, V. V. Srdić, M. G. Antov, J. Serb. Chem. Soc 79 (2014) 533 (http://dx.doi.org/10.2298/jsc131004154i )

2.	M. Ghaedi, A. Ghaedi, F. Abdi, M. Roosta, R. Sahraei, A. Daneshfar, Journal of Industrial and Engineering Chemistry 20 (2014) 787 (http://dx.doi.org/10.1016/j.jiec.2013.06.008)

3.	B. Hameed, L. Chin, S. Rengaraj, Desalination 225 (2008) 185 (http://dx.doi.org/10.1016/j.desal.2007.04.095)

4.	A. K. Kodoth, V. M. Ghate, S. A. Lewis, V. Badalamoole, Int. J. Biol. Macromol. 115 (2018) 418 (http://dx.doi.org/10.1016/j.ijbiomac.2018.04.069)

5.	S. Iftekhar, V. Srivastava, M. Sillanpää, Chem. Eng. J. 309 (2017) 130 (http://dx.doi.org/10.1016/j.cej.2016.10.028)

6.	A. Çiçek, O. Yılmaz, O. Arar, J. Serb. Chem. Soc. 83 (2018) 1059 (http://dx.doi.org/10.2298/JSC170930020C)

7.	O. C. Larbi, H. Merine, Y. Ramli, F. B. Toumi, K. Guemra, A. Dehbi, J. Serb. Chem. Soc. 83 (2018) 1243 (http://dx.doi.org/10.2298/jsc171112065la)

8.	M. R. Avadi, A. M. M. Sadeghi, N. Mohammadpour, S. Abedin, F. Atyabi, R. Dinarvand, M. Rafiee-Tehrani, Nanomedicine: Nanotechnology, Biology and Medicine 6 (2010) 58 (http://dx.doi.org/10.1016/j.nano.2009.04.007)

9.	H. A. Panahi, S. Nasrollahi, Int. J. Pharm. 476 (2014) 70 (http://dx.doi.org/10.1016/j.ijpharm.2014.09.043)

10.	K. Takemasa, S. Kenji, M. Yasunori, J. Control. Release 20 (1992) 3 (http://dx.doi.org/10.1016/0168-3659(92)90133-c)

# Footnotes

Corresponding author. E-mail: alimoghimi@iauvaramin.ac.ir